## Slide 1
Agar-derived Carbon Aerogels
for use in structural EDLCs
Benjamin R. Luginbuhl
Mentor: Cindy Browder, PhD
Northern Arizona University
Department of Chemistry and Biochemistry

## Slide 2: Electric Double-layer Capacitors (EDLCs)
batteries
capacitors
Toxic materials
Slow to charge
High energy density; low power density
Long lifetime
Can be overcharged
Quick to charge
High power density, low energy density
Short lifetime
supercapacitors
Quick to charge, quick to discharge
Cheap to produce
Long lifetime
High power density
Low energy density

## Slide 3: Electric Double-layer Capacitors (EDLCs)
cathode
+ ion
porous separator
- ion
anode
electrolyte matrix
"Electric double-layer capacitor (Activated carbon electrode - BOX type)" by Tosaka - Own work. Licensed under CC BY 3.0 via Wikimedia Commons
Power!

## Slide 5
Carbon Aerogel
conductive
extremely high surface area
produced using a multi-step procedure, toxic chemicals, and very sensitive conditions
Ren and Cheng, Nature 2013

## Slide 6: This Project:
Can we use an alternative material that is cheap, easy, and sustainable to make high surface area carbon aerogel?
Will this alternative carbon aerogel increase the capacitance of structural EDLCs?
structural : device is designed to provide mechanical strength in addition to storing electrical power
Composite material – layered carbon fiber
Solid-polymer electrolyte

## Slide 7: Biopolymer: Agar
+
+
http://www.chemistryland.com/CHM107Lab/Lab5/WaterTest/Lab5Exp1water.html
Magnascan/bigstock.com; Check Man, Cross Man and Jump Man © ioannis kounadeas - Fotolia.com
=
A Hydrogel
powdered polysaccharide
water
heat

## Slide 8: Parameters
Concentration of Agar in water
Gelation time
Drying method Pyrolysis
2 %
3 %
4 %
2 h
3 h
5 h
10 h
Supercritical CO2
Lyophilization
600 °C in 5% H2/Ar, 1.5 min
900 °C in Ar, 30 min

## Slide 9
hydrogel
lyophilize
supercritical dry
cryogel
aerogel
pyrolyze
carbon aerogel

## Slide 10: Pyrolysis
600 °C under 5% H2/Ar for 1 min 30 sec
or
900 °C under Ar for 30 min

## Slide 11: Characterization
Quantitative
Qualitative
Scanning Electron Microscopy (SEM)
Transmission Electron Microscopy (TEM)
BET Surface Area Analysis (SAA)
Cyclic Voltammetry (CV)

## Slide 12: Cryogels (lyophilized)
Type | Surface Area (m2/g)
2 % | 11.0
3 % | -
4 % | 23.3
2 h | -
5 h | 51.8
10 h | 65.1
1 mm

## Slide 13: Aerogels (CPD)
Type | Surface Area (m2/g)
2 % | 241
1 μm

## Slide 14: Carbon Aerogels
Type |  | Surface Area (m2/g)
2 % | Cpd | -
 | Lyo | 715*
3 % | Lyo | -
4 % | Lyo | -
2 h | Lyo | -
5 h | Lyo | -
10 h | LYO | -
6 μm

## Slide 15: TEM Image of Carbon Aerogel
1 μm

## Slide 16
Incorporation Into Device
Electrolyte solution

## Slide 17
Chart: Capacitance of Structural EDLCs
| w/o carbon aerogel | w/ carbon aerogel
2% | 4.3 | 40

## Slide 18
Conclusions
Agar can be used to make high surface area carbon aerogel
There does not appear to be a relationship between the surface area of the cryo/aerogel and the surface area of the resultant carbon aerogel
Initial testing indicates a significant (approx. 10-fold) increase in capacitance when carbon aerogel is incorporated into structural EDLCs

## Slide 19
Next Steps
Continue CPD trials to fill in data
Perfect incorporation method to minimize electrical shorting
Measure other electrical performance metrics (leakage resistance, power density, etc.)

## Slide 20
Acknowledgements
Dr. Cindy Browder
Northern Arizona University
Department of Chemistry and Biochemistry
Brett Cutler
Dr. Nadine Barlow and Kathleen Stigmon
Northern Arizona University
Arizona Space Grant Consortium
Dr. MaryLynn Quartaroli
Northern Arizona University
Hooper Undergraduate Research Award
Aubrey Funke
Northern Arizona University
Imaging & Histology Core Facility
David Wright
Arizona State University
LeRoy Eyring Center for Solid State Science

## Slide 22
Chart: Specific Capacitance of Structural EDLCs
| Lyophilized | CPD | Control
2% | 4.3 | 2.5 | 3.5
3% | 2.4 | 4.4 | 1.8
4% | 2 | 2 | 3
2 h | 2 | 2 | 2
3 h | 2 | 2 | 2
5 h | 2 | 2 | 2
10 h | 2 | 2 | 2