## Slide 1: Plasma enhanced atomic layer deposition of ultrathin oxides on graphene
April 18, 2015
Christie J. Trimble, Anna M. Zaniewski, Manpuneet Kaur, and Robert J. Nemanich
Notes: Introduce self, give background on graphene and project goals.

## Slide 2: Plasma enhanced atomic layer deposition
Controlled, self terminating
Even coverage
Plasma exposure can damage graphene
Notes: Explain PEALD and plasma dilemma.

## Slide 3
Samples of graphene on copper are suspended above sample holders with spacing created by silicon wafers
ALD is performed such that growth is achieved on front and back sides
Notes: Explain suspension technique.

## Slide 4: XPS results-front
Chart: Carbon
Chart: Copper
Chart: Aluminum
Cu
Al
Cu
CuO
Notes: Discuss results

## Slide 5: XPS results-back
Chart: Carbon
Chart: Copper
Chart: Aluminum
Notes: Discuss results

## Slide 6: Raman spectroscopy
Chart: Front of Sample
Chart: Graphene on Copper
Plasma induced defects are found on the front side of the sample but are absent on the back
G
G’
D
G
G’
G
G’
Notes: Discuss results

## Slide 7: Atomic force microscopy results
front
back
Notes: AFM results.

## Slide 8: Next steps
Optimization of ALD results
Transfer of films to TEM grids for further analysis
Notes: Next steps.

## Slide 9: Acknowledgements
Dr. Robert Nemanich, Dr. Anna Zaniewski, Manpuneet Kaur, and the NSL Group
This work was supported by the National Science Foundation and the ASU/NASA Space Grant Program
Notes: Thank you.