## Slide 1: Photo-Induced Au versus Ag Deposition on Periodically Poled Lithium Niobate: Concentration Dependence
Veronica Meeks
Anna Zaniewski, Brandon Palafox, Robert Nemanich
Arizona Space Grant Symposium
April 18th 2015

## Slide 2: Motivation
High demand for metal nanostructures
Unique electrical and optical properties
Utilizing new technique of depositing gold nanoparticles onto periodically poled lithium niobate (PPLN) using ultraviolet (UV) light

## Slide 3: Production

## Slide 4: Analysis

## Slide 5: Results
Chart: Average Diameter (nm)
| 1.10 E -3 | 5.51 E -4 | 2.76 E -4 | 1.00 E -5 | 1.80 E -6 | 1.00 E -7 | 9.10 E -7 | 2.00 E -8
Number per um2 | 0.126 | 1.102 | 1.1 | 1.23 | 15.995 | 10.05 | 0.793 | 0.167
Average Diameter (nm) | 386.9 | 269.5 | 259.67 | 180.08 | 67.39 | 69.92 | 152.62 | 169.9

## Slide 6: Interpretation
Gold Ion Reduction:
Silver Ion Reduction:

## Slide 7: Next Steps
Looking into the physics of the gold concentration graph
Analyze deposition patterns of other metal solutions such as copper

## Slide 8: Acknowledgments
In collaboration with Anna Zaniewski, Robert Nemanich, Brandon Palafox
Funding from ASU/NASA Space Grant Program and the National Science Foundation