## Slide 1: Adsorption of Toxic Metals and Metalloids onto Engineered Nanomaterials
John Lee
Dr. Reyes Sierra
The University of Arizona
Arizona State University Symposium
Tempe, Arizona
April 22nd 2017

## Slide 2: What Are Engineered Nanoparticles (ENPs)?
1 mm
Mount Everest
NPs are particles between 1 and 100 nanometers in size
ENPs are intentionally manufactured to fulfill this size and other technical criteria
166 nm
125 nm
Fe2O3
SiO2
Source: wikipedia.org
Source: TheOutline.com
100 nm
Al2O3
Notes: -what are nanoparticles?
-size
-perspective: bic cristal pen, most popular pen, point on pen is 1 mm, comparing average NP of 20 nm to pen tip = length of pen to height of mt. everest
-not everything exists in nature at these sizes
-ENPs are artificially created to be within these sizes, fulfill other criteria desired by the industry
-why are NPs desirable? Size affects function, reactivity,  lead to next slide, where they’re used

## Slide 3: Where Are ENPs Found?
Source: Photos-Public-Domain.com
Source: forbes.com
Source: Telegraph.co.uk
Source: samsung.com
Source: ias.org.in
Catalysts
Sunscreen
OLED and quantum dot displays
Nanomedicine

## Slide 4: What’s The Issue?
Nanoparticle
Metal contaminants
Potential for metals to adsorb onto ENPs
Adsorption will change where metal contaminants end up
  Environment
  In your body
CeO2 Nanoparticles
Lysosome
500 nm
Notes: Toxic risks of heavy metals
-Arsenic is one of the most highly toxic water pollutants
-Few studies exist on the toxicity of gallium and indium
Picture
-CeO2 in cell

## Slide 5: Objective
Source: JQ Soft
Determine ENP affinity for:
arsenic(III), gallium(III), and indium(III)
Source: JQ Soft

## Slide 6: Methods
Kinetics
  Samples were taken over intervals of time
ENP Screening
  Performed with all ENPs
  Two initial concentrations
Adsorption Isotherms
  Measuring a single ENP with one contaminant
  Many initial concentrations
ENPs
varying mass
NaHCO3
10 mM, 8 pH
Ambient Air
Incubation (shaken, 150 rpm, 23.3°C)
Heavy Metal
varying concentrations

## Slide 7: Results
Chart: Kinetic Adsorption Test
| 72 | 48 | 24 | 8 | 2 | 0.5 | 0.16666666666666666
CeO2 | 0.0485 | 0.0605 | 0.0335 | 0.051 | 0.0815 | 0.298 | 0.915
ZrO2 | 8.5655 | 8.467 | 8.783 | 9.489 | 10.2435 | 10.603 | 11.4045
SiO2 | 12.7095 | 12.5965 | 12.397 | 12.437 | 12.5585 | 12.4205 | 12.3405
Control | 12.206 | 12.122 | 12.204 | 12.062 | 12.264 | 12.125 | 12.378
Adsorption onto ENPs occurs rapidly
Future adsorption experiments will be performed for 48 hours
Chart: Kinetic Adsorption Test
| 72 | 48 | 24 | 8 | 2 | 0.5 | 0.16666666666666666
CeO2 | 0.0485 | 0.0605 | 0.0335 | 0.051 | 0.0815 | 0.298 | 0.915

## Slide 8: Results
Chart: Initial dosing: 0.47 mg Ga/g NP
| CeO2 | Fe | Fe2O3 | TiO2 | Al2O3 | HF-OX-O3 | ZrO2 | SiO2
 | 0.47079 | 0.44399 | 0.43528 | 0.47006 | 0.43803 | 0.4679 | 0.45931 | 0.47695
 | 0.47483 | 0.47483 | 0.47483 | 0.47483 | 0.47483 | 0.47483 | 0.47483 | 0.47483
Chart: Initial dosing: 4.7 mg Ga/g NP
| CeO2 | Fe | Fe2O3 | TiO2 | Al2O3 | HF-OX-O3 | ZrO2 | SiO2
 | 4.3789 | 1.6717 | 3.3089 | 3.5576 | 3.0966 | 2.6985 | 2.7187 | 4.6349
MAX | 4.712 | 4.712 | 4.712 | 4.712 | 4.712 | 4.712 | 4.712 | 4.712
A sufficient amount of ENPs cause complete adsorption of Ga
Gallium was almost fully adsorbed by CeO2 and SiO2

## Slide 9: Conclusions
The three metals have high affinities for many ENPs
  As(III): CeO2, Fe, Fe2O3
  Ga(III): CeO2, SiO2
  In(III): CeO2, TiO2
Focus future research on the impact of ENP-metal interactions for ENP fate, toxicity, and remediation

## Slide 10: Acknowledgements
Dr. Reyes Sierra
Dr. Chao Zeng
The Arizona/NASA Space Grant Consortium through NASA traineeship grant NNX10AI41H

## Slide 11: Thank you