## Slide 1: Evaluation of Force-Sensing Materials for a Small Robotic Gripper
Anna Martin, Mechanical Engineering
Mentor: Dr. Spring Berman
School for the Engineering of Matter, Transport and Energy
Arizona State University

## Slide 2: overview
Autonomous robots will have to sense the amount of force their robotic arm applies to an object, determine if that force is too high or too low, and adjust its force output accordingly.
Force Sensing Resistors (FSRs) were previously tested for precision, accuracy, and ease of use and were determined to be too rigid
Cheaper materials, such as velostat, anti-static foam, and neoprene-copper were tested
Applications in robotics: construction and assembly, repairing damaged equipment, load manipulation
Notes: Test bed finalized

## Slide 3: The problem with fSRs
Too rigid
Did not conform to the shape of the manipulator’s jaws
Poor leads did not allow for easy connection to other wires
  Led to wires disconnecting during testing, which led to incomplete data
Cost
  $14 per sensor
  Each manipulator requires 2 sensors, becomes costly for a swarm of robots

## Slide 4: The candidates for the material
Material | Cost | Performance
Anti-static foam | $0.00 because the material was already present in the lab | Large amount of noise (in the MΩ range at times)
Velostat | $0.016 for.71*.71” square | Not as consistent for lower amounts of force; easy to assemble; better if more than one layer is used
Neoprene-copper | $0.079 for .71*.71” square | Difficult to assemble; only conducted on outer edges, most likely due to error in assembly process

## Slide 5: The test bed
Original Design
New Design
Wires
Sensor material
Weights
Arduino Mega
Material mounts double as wire holders

## Slide 6: Test bed results for fsr and velostat
Consistency between trials
Comparing materials
Notes: Curve-fitted equation for 2 layers: R = -21.9556*F + 1.2699e3, F in Newtons, R in Ohms. Solve for F: F = -.045546*R + 57.8395

## Slide 7: Implementation on a manipulator
Advantages:
  Velostat fit the gripper’s jaws well
  Wires can be positioned any way
Disadvantages:
  Alligator clips added weight to wires and moved them
  Wires are still too rigid and would slip out of mounting putty
  Difficult to assemble
    Had to take apart gripper
    Everything would move as soon as it was reassembled

## Slide 8: Data comparison between fsrs and velostat sensors
FSR
Velostat
The wires from the force sensors kept getting displaced once the manipulator’s jaws squeezed the paddles, so data could not consistently be obtained
When data could be obtained, there were still large variabilities between the readings of the left and right sensors
  Likely due to human error in the placing of the sensors
Trial | Average Left FSR Reading | Average Right FSR Reading
1 | 0.330137 | 1.980386
2 | 0.766734 | 3.372041
3 | 4.586414 | 4.69143
4 | 2.401946 | 3.197892
5 | 1.959711 | 4.532586
6 | 2.89983 | 3.64819
7 | 2.054446 | 1.430803
8 | 1.75455 | 3.644629
9 | 2.219138 | 3.862424
10 | 2.626148 | 3.042145
11 | 2.026046 | 2.162665
12 | 2.557159 | 2.281657
13 | 3.070709 | 1.354307
14 | 1.866366 | 1.075359
15 | 3.426502 | 4.778084

## Slide 9: Conclusions and future developments
What I Learned
Consider wires in design
Force-response in various materials is still a research-heavy field
Force sensors made with Velostat are cheaper than traditional FSRs while retaining many properties of FSRs
Because the sensors were hand-made, it was difficult to consistently make them exactly the same, leading to inconsistencies in readings
Future Applications
New jaw design with custom force sensor integrated
  Keep wires stationary
  Protect Velostat and wiring
  More professional look
Force feedback system

## Slide 10: acknowledgements
Dr. Spring Berman, Department of Mechanical and Aerospace Engineering
Ruben Gameros, Research Specialist, Department of Mechanical and Aerospace Engineering
Sean Wilson, Ph.D. student, Department of Mechanical and Aerospace Engineering

## Slide 11: Questions?