## Slide 1: Normal Stress Developing in Magnetorheological (MR) Fluids.
Nikki Cain
Northern Arizona University
Mentor: Constantin Ciocanel, PhD
Department of Mechanical Engineering

## Slide 2: Background
Understand the normal stress developing in magnetorheological fluids (MRF)
MRF
  Smart material made of a carrier fluid and iron-based micron size particles
  Magnetic field yields an apparent viscosity increase
What is known:
  Shear force on particle chains
  Flow mode “Valve Mode”
What is sought:
  Normal force on particle chains
  “Squeeze Mode”
Figure 1: MRF particles reacting to magnetic field application [1]

## Slide 3: Applications of MRF
Flow Mode
  Shock absorbers
Shear Mode
  Clutches and Breaks
Squeeze Mode
  Controlling small movements
  Large forces
Figure 2: MRF Shock absorber [2]
Figure 3: MRF Clutch/break design [3]

## Slide 4: Introduction
Determine magnitude of the normal stress as a function of magnetic field strength, gap size, temperature, and frequency of squeezing
Others have attempted to validate normal force models with experimental data
  Normal stress and normal forces
  Yielding behavior and stress differences
Model predictions will be compared to experimental data
Figure 4: MRF Chain Model and Normal Force Equation [4]

## Slide 5: Experiment
Rheometer
  Laboratory device used to measure fluid properties such as viscosity, shear stress and normal stress
  Magnetorheological accessories/electromagnet
Gaussmeter
  Measures magnetic field strength
Thermocube
  Electromagnet’s cooling unit
Measure the normal stress that develops in different amounts of fluid exposed to different magnetic field strengths.
Figure 5: Rheometer with MRF loaded between the plates.

## Slide 6: Experiment
Figure 6: MRF Enclosure ready for testing
Gaussmeter
Coolant lines
Electromagnet/
Lower plate
MRF’s enclosure

## Slide 7: Results
0.3 mL MRF, 0.25T, 950mm max gap
0.6 mL MRF, 0.25T, 1910mm max gap
0.9 mL MRF, 0.25T, 2860mm max gap
- Gap effect on Normal stress magnitude

## Slide 8
Results
0.6 mL MRF, 0.25T, 1910mm max gap
0.6 mL MRF, 0.5T, 1910mm max gap
0.6 mL MRF, 0.75T, 1910mm max gap
- Field effect on Normal stress magnitude in 0.6 mL of fluid

## Slide 9
Results
0.9 mL MRF, 0.25T, 2860mm max gap
0.9 mL MRF, 0.5T, 2860mm max gap
0.9 mL MRF, 0.75T, 2860mm max gap
- Field effect on Normal stress magnitude in 0.9 mL of fluid

## Slide 10: Conclusions
What was found
  The smaller the gap and the higher the field, the larger the normal stress
  Decreasing the gap below 1.4 mm doesn’t yield a much higher increase in normal stress, but limits the travel of the boundaries squeezing the fluid, hence limiting the range of applications of the fluid
Moving Forward
  Additional experimental data needs to be collected, particularly under oscillatory squeeze mode
  Compare existing model predictions with experimental data for all analyzed cases and identify missing features in the model to allow for accurate predictions

## Slide 11: Acknowledgements
NASA Space Grant and Arizona Space Grant Consortium
Constantin Ciocanel, PhD
Timothy Becker, PhD and William Merritt (Bill)

## Slide 12: Questions?

## Slide 13: References
[1]"MAGNETORHEOLOGICAL FLUIDS AND DEVICES", Mrfengineering.com.ua, 2018. [Online]. Available: http://mrfengineering.com.ua/en/magnitoreologicheskaya-zhidkost.
[2] "SHOCK ABSORBER PASSION REAR SET ENDURANCE- Motorcycle Parts For Hero Honda Passion", Safexbikes Motorcycle Superstore, 2018. [Online]. Available: https://safexbikes.com/productdetail/motorcycle-parts/shock-absorbers/hero-honda-passion/S135104407.
[3]"Research of Kikuchi Lab", Www2.hwe.oita-u.ac.jp, 2018. [Online]. Available: http://www2.hwe.oita-u.ac.jp/kikuchilab/Research/Research_eng.html.
[4] H. Laun, C. Gabriel and G. Schmidt, "Primary and secondary normal stress differences of a magnetorheological fluid (MRF) up to magnetic flux densities of 1T", Journal of Non-Newtonian Fluid Mechanics, vol. 148, no. 1-3, pp. 47-56, 2008.