## Slide 1: Deposition of Alkanethiolate Self-Assembled Monolayers on Germanium
ViAnn Pham1
Stacy Heslop2, Anthony Muscat1
Department of Chemical and Environmental Engineering1
Department of Chemistry and Biochemistry2
University of Arizona
NASA Space Grant Symposium
University of Arizona - Tucson
Saturday, April 14, 2018

## Slide 2: Motivation and Background
Problem: Ge form unstable oxides that inhibit device performance.
  Need to find effective surface passivation method for Ge at reasonable time scales
  Passivation layer = coat of protective material that reduces the amount of chemical reactivity on the surface
2
Material | Hole Mobility (cm2 V/s)
Silicon | 200
Germanium | 450
https://www.androidcentral.com/sites/androidcentral.com/files/styles/xlarge/public/article_images/2015/01/Transistor.png
Del Alamo, Jesús A. "Nanometre-scale electronics with III-V compound semiconductors." Nature 479.7373 (2011): 317-323.

## Slide 3: Motivation and Background
Use octadecanethiol (ODT) as passivation reagent.
  Long-chain thiol
  Used successfully in literature, but at long time scales (20 h)
    Not practical for industry
Goal: reduce passivation time by adding ethylenediamine (EDA)
3
Ge
EDA converts thiol to thiolate.

## Slide 4: Adding amine increases layer thickness
4
Ideal overlayer thickness

## Slide 5: Objective
Goal: Reduce the deposition time of a dense, highly-ordered alkanethiolate passivation.
Ge
Alkanethiolates
Control
Alkanethiolate-passivated surface
Ge
5

## Slide 6: Procedure
Cleaning and etching
SC-1 or sonication
HF/HCl Oxide strip 5 min
Control
N2 dry
Passivation
4 mM ODT in EtOH
  w/ EDA (1.5 -150 mM)
  RT vs 60°C
  20 min vs 20 h
SiGe 75%
Ge
Ge
alkanethiolates
Ge
SiGe 75%
GeO2
Ge
6

## Slide 7: Characterization
Spectroscopic ellipsometry
Measured overlayer (oxides) thickness
X-ray photoelectron spectroscopy (XPS)
Determine chemical species on surface.
Wikipedia
Wikimedia Commons
6

## Slide 8: Amine increases carbon coverage
Amine does not oxidize the surface.
Concentration of amine does not affect coverage
7

## Slide 9
8
At 20 h, thiol and amine solutions show a decrease in the C/Ge ratio than just thiol alone.
For 20 h immersion, amine decreases C/Ge ratio

## Slide 10: Increasing temperature with amine decreases C/Ge ratio
Increasing temperature increase C/Ge ratio for thiol alone, but decreases C/Ge ratio for thiol and amine solutions.
9

## Slide 11: Overlayer thickness corroborates XPS results
10
With EDA, increasing T  Lower thickness
At 60°C, adding EDA  Lower thickness
At RT, adding EDA  higher thickness
ODT alone, increasing T  higher thickness

## Slide 12: Conclusions
EDA helps at RT and does not contribute to oxidation.
20 h immersion produces a more dense and highly-ordered layer than 20 min immersion
Increasing temperature for solutions with EDA does not produce a more dense and highly-ordered layer.
Future Work
Confirm temperature trends.
12
Notes: .

## Slide 13: Acknowledgements
Muscat Research Group
NASA/Arizona Space Grant Consortium
Lam Research
13

## Slide 14: Thank you!
14