## Slide 1: Wadsleyite Synthesis for Laser Driven Shock Experiments
By: Jacqueline Tappan
Mentors: S.-H. Dan Shim & Kurt Leinenweber
School of Earth and Space Exploration
ASU

## Slide 2: Laser Driven Shock
Laser beams shock material producing high pressure and temperature conditions similar to those found in the deep interiors of the Earth or in large Earth-like exoplanets.
Shock experiments require a dense starting material to then transform to its high pressure polymorph.
If a less dense material is used, upon shock, the material will act as a fluid.
Forsterite Wadsleyite High Pressure Polymorph
Increasing pressure

## Slide 3: Synthesizing Wadsleyite
Forsterite Wadsleyite
Synthetic forsterite (Mg2SiO4) was used as a starting material
A high pressure/high temperature multi-anvil press was then used to apply desired conditions to the sample

## Slide 4: Multi-Anvil Press
6-8 Kawai and Endo type Multi Anvil was used in this experiment at Arizona State University
6 steel wedges and 8 Tungsten Carbide cubes
The National Centre of Experimental Mineralogy and Petrology. (n.d.). Retrieved from http://ncemp.org/MultiAnvil.htm

## Slide 5: A look Inside the Assembly
(Mgo)
Nesting Plates

## Slide 6: 14/8 Assembly
14/8 refers to the edge length of the octahedron and the truncation on the tungsten carbide cubes.
14mm = Octahedron edge length 8mm = Truncation Length
14mm
8mm

## Slide 7
Run Conditions
1150o C
14 GPa
dwell for 2 hours before quenching
Burnley , P. (2016, November 15). Phase Equilibria at High Pressure
= Run Conditions plotted on Mg2SiO4 Phase Diagram

## Slide 8: Results
A total of 5 multi-anvil runs were done at these conditions, each checked with Raman Spectroscopy to confirm that they were indeed wadsleyite
3mm
3mm
3mm
3mm
3mm

## Slide 9: Raman Spectrum
http://rruff.info/wadsleyite/display=default/

## Slide 10: Future Research
Synthesizing Akimotoite, Majorite, and Bridgmanite at different conditions to understand the triple point in the MgSiO3 system.