## Slide 1: Investigating geopolymer-mediated adsorption of MRSA cells and secreted proteins
Collin Ganser
Dr. Shelley E. Haydel – The Biodesign Institute Center for Immunotherapy, Vaccines and Virotherapy
Shaojiang Chen and Dr. Dong-Kyun Seo – The Biodesign Institute Center for Molecular Design and Biomimetics
4-13-19
Arizona NASA Space Grant Statewide Symposium

## Slide 2: MRSA
Methicillin-resistant Staphylococcus aureus
Major cause of skin and soft tissue infections
Difficult to treat due to antibiotic resistance
Fritz, A. L., & Jasmer, R. (2018). Everything You Need to Know About the Superbug, MRSA | Everyday Health.

## Slide 3: Alternative Treatment Methods
Antimicrobial peptides
Metal ions
  Microzeolites
  Nanozeolites
Bahar, A. A., & Ren, D. (2013). Antimicrobial Peptides. Pharmaceuticals,6(12), 1543-1575.

## Slide 4: Geopolymers
Aluminosilicate materials
Contain cage-like structures that act as pores
Can alter pore size
  macro vs. meso
Can alter surface chemistry
  non-coated vs. stearic acid-coated

## Slide 5: Methodology
Tested geopolymers adsorption capability of whole cells and secreted proteins (culture filtrate proteins [CFP])
Basic idea: isolate adsorption target and incubate with geopolymers

## Slide 6: MRSA Whole Cell Adsorption
Grew MRSA in tryptic soy broth and resuspended in saline
Incubated MRSA cells with 10, 5, and 0 mg/mL GP for 1 h
Separated unbound MRSA from GP with filter
Plated unbound MRSA to quantify GP adsorption

## Slide 7: Whole Cell Adsorption Results

## Slide 8: Secreted MRSA Protein Adsorption
Grew MRSA in chemically defined medium to generate CFP
Separated CFP from MRSA to remove whole cells
Incubated CFP with GP for 1 h to test adsorption capabilities
Resolved on SDS-PAGE to compare CFP incubated with and without GP

## Slide 9: Secreted Protein Adsorption Results
L
2.7
GP
μg/mL CFP
6.8
13.6
27
CDM
- +
- +
- +
- +

## Slide 10: Conclusions
Geopolymers’ ability to adsorb whole MRSA cells:
  macroGP > SA-macroGP > SA-mesoGP > mesoGP
SA-macroGP (1 mg/mL) does not adsorb MRSA CFP (2.7-27μg/mL)

## Slide 11: Future Directions
Compare different concentrations and types of GP for CFP adsorption
If GP adsorbs MRSA CFP, perform mass spectrometry to identify adsorbed proteins

## Slide 12: Acknowledgements
Dr. Shelley E. Haydel
John Popovich
Michelle McBride
Shaojiang Chen
Dr. Dong-Kyun Seo
ASU/NASA Space Grant
School of Life Sciences Undergraduate Research (SOLUR) Program

## Slide 13: Thank You!
Questions?