## Slide 1: Emerging Non-Volatile Memory: Resistive Switching Behaviors in Amorphous Tungsten Oxide Dielectric
Maxwell Weiss
Supervisor: Dr. Ying-Chen Chen
Northern Arizona University
Department of Electrical Engineering
NASA Space Grant Symposium

## Slide 2: Outline
Motivation
Experimental Methods
Results and Discussion
Conclusion and future work

## Slide 3: Motivation
There exists a speed gap between fast, volatile memories (i.e. DRAM,SRAM) and slow, non-volatile memory (i.e. Flash).
We want to find the next generation memory to improve upon Flash speed, reliability, and scalability
Source: An Chen, A review of emerging non-volatile memory (NVM) technologies and applications, Solid-State, Electronics, Volume 125, 2016.
Transistor based Flash memory cannot scale down to smaller feature sizes due to increasing charge loss (i.e data loss).
Meena, Jagan & Sze, Simon & Chand, Umesh & Tseng, Tseung-Yuen. (2014). Overview of Emerging Non-volatile Memory Technologies. Nanoscale Research Letters. 9. 1-33.

## Slide 4: Experimental Method-Thin Film
***All films deposited by electron-beam physical vapor deposition at Torr
Fabrication Procedure
Probing Side View
View from probe station camera.
Probing Top-Down View
Data extracted with Semiconductor Device Analyzer [Keysight B1500A]

## Slide 5: Experimental Method: Nano-Helix Films
Length: 50,100, 200 nanometers
Pitch (turn length): 50 nanometers
Sumant Sarkar, Ryan O. Behunin, and John G. Gibbs Nano Letters 2019
Geometry of a Nano-Helix
Michael T. Taschuk et. al. Chapter 13 - Glancing Angle Deposition, Handbook of Deposition Technologies for Films and Coatings
Glancing Angle Deposition Method

## Slide 6: Results and Discussion
20 devices tested for 3 thicknesses of 50, 100, and 200 nanometers
For each device 20 switching cycles occurred
Conductive Filament Theory
Electroforming: Form the percolation path (soft-breakdown).
Reset: Oxygen ions () drift back and oxidize
Set: Generation oxygen vacancies (
Ye, Cong et. al Applied Physics Express (2014)
1
2
3
4
5

## Slide 7: Results and Discussion
Memory Window increases with decreasing thickness.
Operation voltage are below +/-1V (SET/RESET) for low power applications.
High endurance is demonstrated with 200 DC sweep cycles without significant memory drop.
Unpublished results, paper in progress

## Slide 8: Optical Analysis and Observations
Positive CD indicates right-handed helixes.
Joule heating induced annealing
Tauc’s Relation
Bouguer-Lambert Law
Thickness=50nm
R. Sivakumar, et. al. Optical Materials, Volume 29, Issue 6, 2015
Sumant Sarkar, Ryan O. Behunin, and John G. Gibbs Nano Letters 2019

## Slide 9: Conclusion and Future Work
Key Points
The SET/RESET voltage of device are below +/- 1V.
Memory window is approximately and decreases with increasing WOx thickness.
Reset voltage decreases with WOx thickness.
Devices are sensitive to high current induced annealing.
Future Work
Comparison of memory characteristics between nano-helix and thin film devices.
Investigation of data retention performance.
Utilizing X-Ray Photoelectron Spectroscopy and Energy Dispersive Spectroscopy to characterize material characteristics.

## Slide 10: Acknowledgements
Dr. Ying-Chen Chen
Dr. John Gibbs
Dr. Sumant Sarkar
School of Informatics Computing and Cyber Systems
Semiconductor Device and Research Lab
Center for Materials Interfaces in Research and Applications

## Slide 11: Thank you Questions?