## Slide 1
Investigation of Stress Concentrations in Parts Manufactured with Fused Deposition Modeling
Hope Elmer and Alexandre Lasalarie
Mentor: Dr. David Lanning
College of Engineering
Department of Aerospace Engineering
Arizona NASA Space Grant Statewide Symposium
Tempe, AZ

## Slide 2
Fused Deposition Modeling (FDM),
a type of 3D printing, is highly customizable
Process:
Parameters:
Source: Ahn, D., Kweon, J., Kwon, S., "Representation of surface roughness in fused deposition modeling," Journal of Materials Processing Technology, Vol. 209, No. 15, 2009, pp. 5593-5600.
Solid Base Layer
Solid Top Layer
Gyroid Infill
Perimeter

## Slide 3
Effects of stress concentrations
in FDM parts has yet to be studied
Source: McGinty, B., “Stress Concentrations at Holes,” Stress concentrations at holes Available: https://www.fracturemechanics.org/hole.html.

## Slide 4
The studied specimens have equal
theoretical stress concentrations across the widths
Theoretical K
2.5
2.4
2.2

## Slide 5
The specimens are tested in tension until failure

## Slide 6
Failure location deviates from predicted location
20% Infill Density
60% Infill Density

## Slide 7
Experimental data contradicts theory
Chart: HOLE
| 1 | 1.5 | 2
20% | 2673.2093 | 2061.267 | 1856.1852
40% | 3435.05 | 2511.531 | 2416.1814
60% | 3784.442 | 3374.2012 | 2964.4045
failure away from hole | 2673.2093 | 2061.267 | 1856.1852 | 2511.531
Chart: NOTCH
| 1 | 1.5 | 2
20% | 1822.4987 | 1476.4564 | 1363.053
40% | 2497.9152 | 2283.7412 | 2033.0606
60% | 3314.2657 | 2963.7288 | 2778.5547

## Slide 8
The difference between stresses is reduced
by taking the stress with respect to the ‘shell’
Chart: Width [in]
| 1 | 1.5 | 2
20% | 7026.5651 | 6544.049 | 6459.2845
20% | 6976.5578 | 7184.5432 | 7374.905
40% | 9613.5634 | 10080.0994 | 9622.0671
40% | 9115.1921 | 8746.5478 | 9602.4329
60% | 12750.948 | 13095.1297 | 13185.6916
60% | 10079.5655 | 11794.1911 | 11799.8782
Hole
Notch
20%
40%
60%

## Slide 9
The experimental K values for both
specimens are lower than the theoretical K value
Chart: NOTCH
| 0.26981597239217114 | 0.20206655053714856 | 0.15150528042550773
20% | 1.1155 | 1.377 | 1.4918
40% | 1.3345 | 1.4597 | 1.6396
60% | 1.1725 | 1.3112 | 1.3704
Theory | 2.894 | 2.7283 | 2.5683 | 2.4142 | 2.2664 | 2.1251 | 1.9908 | 1.8636 | 1.7438 | 1.6319 | 1.528 | 1.4325 | 1.3457 | 1.2679 | 1.1994 | 1.1405 | 1.0915 | 1.0527
Chart: HOLE
| 0.38769159159912697 | 0.26006204366082408 | 0.19510777292471496
20% | 0.76086 | 0.98522 | 1.0953
40% | 0.97044 | 1.3551 | 1.3797
60% | 1.0268 | 1.1516 | 1.3108
Theory | 2.86 | 2.7319 | 2.6185 | 2.519 | 2.4324 | 2.3576 | 2.2936 | 2.2395 | 2.1943 | 2.157 | 2.1266 | 2.1021 | 2.0825 | 2.0668 | 2.0541 | 2.0434 | 2.0336 | 2.0237 | 2.0129