## Slide 1: Carbon Dioxide Capture in Spacecraft Using Novel Microsphere-loaded Polymers
Cameron Morgan
Associate Professor Matthew Green
School for Engineering of Matter, Transport & Energy
Mentors: Ani Nazari & Kacie Niimoto
NASA Space Grant Symposium 2023

## Slide 2
Motivation
  Problems
  Elevated CO2 levels lead to adverse health affects
  Zeolite issues: dusting and water uptake
  High temperature regeneration, which is not energy efficient
  Necessary requirements: high efficiency, low energy usage, high structural strength, no dusting with water
  Research Question
  How does the addition of Expancel microspheres impact a polymer designed for CO2 capture, using a humidity-swing system?
  Addition of the spheres likely increases the available active sites for CO2 capture
    Expand until rupture – makes porous foam structure
    Expanded spheres, increase surface area
  Dry Unexpanded (DU) vs Dry Expanded (DE) Microspheres
Figure 1: Microsphere expansion graphic from Nouryon.
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work
1
Figure 2: Dry microspheres image from Nouryon.

## Slide 3
Motivation
Figure 1: Microsphere expansion graphic from Nouryon.
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work
1
  Problems
  Elevated CO2 levels lead to adverse health affects
  Zeolite issues: dusting and water uptake
  High temperature regeneration, which is not energy efficient
  Necessary requirements: high efficiency, low energy usage, high structural strength, no dusting with water
  Research Question
  How does the addition of Expancel microspheres impact a polymer designed for CO2 capture, using a humidity-swing system?
  Addition of the spheres likely increases the available active sites for CO2 capture
    Expand until rupture – makes porous foam structure
    Expanded spheres, increase surface area
  Dry Unexpanded (DU) vs Dry Expanded (DE) Microspheres
Figure 2: Dry microspheres image from Nouryon.

## Slide 4
Motivation
Figure 1: Microsphere expansion graphic from Nouryon.
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work
1
  Problems
  Elevated CO2 levels lead to adverse health affects
  Zeolite issues: dusting and water uptake
  High temperature regeneration, which is not energy efficient
  Necessary requirements: high efficiency, low energy usage, high structural strength, no dusting with water
  Research Question
  How does the addition of Expancel microspheres impact a polymer designed for CO2 capture, using a humidity-swing system?
  Addition of the spheres likely increases the available active sites for CO2 capture
    Expand until rupture – makes porous foam structure
    Expanded spheres, increase surface area
  Dry Unexpanded (DU) vs Dry Expanded (DE) Microspheres
Figure 2: Dry microspheres image from Nouryon.

## Slide 5
Motivation
Figure 1: Microsphere expansion graphic from Nouryon.
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work
1
  Problems
  Elevated CO2 levels lead to adverse health affects
  Zeolite issues: dusting and water uptake
  High temperature regeneration, which is not energy efficient
  Necessary requirements: high efficiency, low energy usage, high structural strength, no dusting with water
  Research Question
  How does the addition of Expancel microspheres impact a polymer designed for CO2 capture, using a humidity-swing system?
  Addition of the spheres likely increases the available active sites for CO2 capture
    Expand until rupture – makes porous foam structure
    Expanded spheres, increase surface area
  Dry Unexpanded (DU) vs Dry Expanded (DE) Microspheres
Figure 2: Dry microspheres image from Nouryon.

## Slide 6
Motivation
Figure 1: Microsphere expansion graphic from Nouryon.
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work
1
  Problems
  Elevated CO2 levels lead to adverse health affects
  Zeolite issues: dusting and water uptake
  High temperature regeneration, which is not energy efficient
  Necessary requirements: high efficiency, low energy usage, high structural strength, no dusting with water
  Research Question
  How does the addition of Expancel microspheres impact a polymer designed for CO2 capture, using a humidity-swing system?
  Addition of the spheres likely increases the available active sites for CO2 capture
    Expand until rupture – makes porous foam structure
    Expanded spheres, increase surface area
  Dry Unexpanded (DU) vs Dry Expanded (DE) Microspheres
Figure 2: Dry microspheres image from Nouryon.

## Slide 7
Motivation
Figure 1: Microsphere expansion graphic from Nouryon.
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work
1
  Problems
  Elevated CO2 levels lead to adverse health affects
  Zeolite issues: dusting and water uptake
  High temperature regeneration, which is not energy efficient
  Necessary requirements: high efficiency, low energy usage, high structural strength, no dusting with water
  Research Question
  How does the addition of Expancel microspheres impact a polymer designed for CO2 capture, using a humidity-swing system?
  Addition of the spheres likely increases the available active sites for CO2 capture
    Expand until rupture – makes porous foam structure
    Expanded spheres, increase surface area
  Dry Unexpanded (DU) vs Dry Expanded (DE) Microspheres
Figure 2: Dry microspheres image from Nouryon.

## Slide 8
Motivation
Figure 1: Microsphere expansion graphic from Nouryon.
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work
1
  Problems
  Elevated CO2 levels lead to adverse health affects
  Zeolite issues: dusting and water uptake
  High temperature regeneration, which is not energy efficient
  Necessary requirements: high efficiency, low energy usage, high structural strength, no dusting with water
  Research Question
  How does the addition of Expancel microspheres impact a polymer designed for CO2 capture, using a humidity-swing system?
  Addition of the spheres likely increases the available active sites for CO2 capture
    Expand until rupture – makes porous foam structure
    Expanded spheres, increase surface area
  Dry Unexpanded (DU) vs Dry Expanded (DE) Microspheres
Figure 2: Dry microspheres image from Nouryon.

## Slide 9
Synthesis & Results
SEM image of 1 % (w/w) dry expanded microspheres
(500 µm scale, 80x magnification)
SEM image of control without microspheres
(400 µm scale, 100x magnification)
Method 1
Expanding Unexpanded Microspheres
Method 2
Using Pre-expanded Microspheres
Objective
Increase surface area to increase the number of available active capture sites
v
v
Surface Area (Unexpanded) < Surface Area (Expanded)
2
Add heat
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work

## Slide 10
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work
Synthesis & Results
SEM image of 1 % (w/w) dry expanded microspheres
(500 µm scale, 80x magnification)
SEM image of control without microspheres
(400 µm scale, 100x magnification)
Method 1
Expanding Unexpanded Microspheres
Method 2
Using Pre-expanded Microspheres
Objective
Increase surface area to increase the number of available active capture sites
v
v
Surface Area (Unexpanded) < Surface Area (Expanded)
2
Add heat
Vial polymerization
UV
Stir bar mixing

## Slide 11
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work
Synthesis & Results
SEM image of 1 % (w/w) dry expanded microspheres
(500 µm scale, 80x magnification)
SEM image of control without microspheres
(400 µm scale, 100x magnification)
Method 1
Expanding Unexpanded Microspheres
Method 2
Using Pre-expanded Microspheres
Objective
Increase surface area to increase the number of available active capture sites
v
v
Surface Area (Unexpanded) < Surface Area (Expanded)
2
Add heat
Vial polymerization
Silicon mold polymerization
UV
Stir bar mixing
UV

## Slide 12
CO2 Testing
Sample | CO2 Uptake at 20 Hours (µmol/g) | CO2 Uptake Kinetics (first 5 hours) (µmol/g*hr-1) | Bicarbonate Exchange (1 soak)
1% (w/w) DE Microspheres (Si mold) | 85.4 | 13.0 | 75.9%
Control (Si Mold) | 57.3 | 6.6 | 75.9%
Control (vial) | 18.3 | 2.34 | 59.4%
1% (w/w) DU Microspheres (vial) | 13.2 | 1.1 | 50.0%
Control without microspheres
1% (w/w) DE Microspheres
Synthesis Method: 1% (w/w)
Pre-expanded DE microspheres
Photopolymerization in silicon mold under UV light
3
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work

## Slide 13
Energy Efficiency
Moisture Swing Regeneration
(simplified)
Zeolite Temperature/Pressure Swing Regeneration
(simplified)
CO2 Capture
Cabin Air
CO2 Desorption
Drying
Re-humidify
Cabin Air
Apply heat/ pressure change
Space vacuum
CO2 Capture
Cabin Air
CO2 Desorption
Drying
Re-humidify
Cabin Air
Increase humidity
Space vacuum
More energy efficient
4
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work

## Slide 14
Energy Efficiency
Moisture Swing Regeneration
(simplified)
Zeolite Temperature/Pressure Swing Regeneration
(simplified)
CO2 Capture
Cabin Air
CO2 Desorption
Drying
Re-humidify
Cabin Air
Apply heat/ pressure change
Space vacuum
CO2 Capture
Cabin Air
CO2 Desorption
Drying
Re-humidify
Cabin Air
Increase humidity
Space vacuum
More energy efficient
4
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work

## Slide 15
Energy Efficiency
Moisture Swing Regeneration
(simplified)
Zeolite Temperature/Pressure Swing Regeneration
(simplified)
CO2 Capture
Cabin Air
CO2 Desorption
Drying
Re-humidify
Cabin Air
Apply heat/ pressure change
Space vacuum
CO2 Capture
Cabin Air
CO2 Desorption
Drying
Re-humidify
Cabin Air
Increase humidity
Space vacuum
More energy efficient
4
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work

## Slide 16
Conclusions and Future Work
Conclusions
Pre-expanded microspheres have good dispersal (as seen in SEM images)
Dry expanded microspheres increases the kinetics of CO2 uptake and sorption capacity
Photopolymerization is best in a silicon mold rather than a vial
Humidity-swing is more energy efficient than current technology
5
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work

## Slide 17
Conclusions and Future Work
Conclusions
Pre-expanded microspheres have good dispersal (as seen in SEM images)
Dry expanded microspheres increases the kinetics of CO2 uptake and sorption capacity
Photopolymerization is best in a silicon mold rather than a vial
Humidity-swing is more energy efficient than current technology
5
SEM image of 1 % (w/w) dry expanded microspheres
(500 µm scale, 80x magnification)
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work

## Slide 18
Conclusions and Future Work
Conclusions
Pre-expanded microspheres have good dispersal (as seen in SEM images)
Dry expanded microspheres increases the kinetics of CO2 uptake and sorption capacity
Photopolymerization is best in a silicon mold rather than a vial
Humidity-swing is more energy efficient than current technology
SEM image of 1 % (w/w) dry expanded microspheres
(500 µm scale, 80x magnification)
Sample | CO2 Uptake at 20 Hours (µmol/g) | CO2 Uptake Kinetics (first 5 hours) (µmol/g*hr-1) | Bicarbonate Exchange (1 soak)
1% (w/w) DE Microspheres (Si mold) | 85.4 | 13.0 | 75.9%
Control (Si Mold) | 57.3 | 6.6 | 75.9%
5
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work

## Slide 19
Conclusions and Future Work
Conclusions
Pre-expanded microspheres have good dispersal (as seen in SEM images)
Dry expanded microspheres increases the kinetics of CO2 uptake and sorption capacity
Photopolymerization is best in a silicon mold rather than a vial
Humidity-swing is more energy efficient than current technology
Silicon mold polymerization
UV
SEM image of 1 % (w/w) dry expanded microspheres
(500 µm scale, 80x magnification)
5
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work

## Slide 20
Conclusions and Future Work
Conclusions
Pre-expanded microspheres have good dispersal (as seen in SEM images)
Dry expanded microspheres increases the kinetics of CO2 uptake and sorption capacity
Photopolymerization is best in a silicon mold rather than a vial
Humidity-swing is more energy efficient than current technology
Silicon mold polymerization
UV
SEM image of 1 % (w/w) dry expanded microspheres
(500 µm scale, 80x magnification)
5
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work

## Slide 21
Conclusions and Future Work
Conclusions
Pre-expanded microspheres have good dispersal (as seen in SEM images)
Dry expanded microspheres increases the kinetics of CO2 uptake and sorption capacity
Photopolymerization is best in a silicon mold rather than a vial
Humidity-swing is more energy efficient than current technology
SEM image of 1 % (w/w) dry expanded microspheres
(500 µm scale, 80x magnification)
Future Work
Varying w/w % of expanded microspheres using a silicone mold with UV platform/photopolymerization
Perform modular strength testing and porosity measurements using SEM images
Integrate microspheres into more types of polymers
Silicon mold polymerization
UV
5
Motivation Synthesis & Results CO2 Testing Energy Efficiency Conclusions & Future Work

## Slide 22
Thank you
6

## Slide 23
Introduction
About me
Junior in Environmental Engineering – needed lots of learning about polymers!
Want to get a PhD and become a professor
Previous research projects
  Mask efficacy published paper, I developed simulations
  Developing multifunctional infrastructure materials able to simultaneously decrease building temperature and remove/degrade air pollutants
  NOx conversion using H2 as a reductant at low temperatures. I synthesized platinum- based catalysts with a novel additive and synthesis method
  Other current involvements
    GCSP
    Fulton Ambassador
    American Society of Civil Engineers – ASU chapter

## Slide 24
Synthesis & Results
Method 1: Expanding pre-cure
Dry unexpanded microspheres
Photopolymerization using DMPA initiator
Method 2: Expanding during cure
Dry unexpanded microspheres
Thermal polymerization using AIBN initiator
Method 3: Pre-expanded photopolymerization
Dry expanded microspheres
Photopolymerization using DMPA initiator
Polymerization Method
Polymerization 1 (top image): UV box
Solution cured in a vial
Polymerization 2 (bottom image): UV platform
Solution cured in silicone mold
Polymerization 3: Oven
Solution cured in silicone mold
(Control, no spheres)
(w/ expanded spheres)
CO2 capture monomer (TMAEMA-Cl- ). Chloride exchanged with DAC functional counter-ion HCO3-
Crosslinking monomer (PEGDMA)

## Slide 25
CO2 Testing
DE microsphere-enhanced polymer (red) displayed fastest kinetics of uptake and highest adsorption
Polymers prepared through method 3 and using the platform for photopolymerization performed much better than those prepared through method 1 and using the vial.
Polymers prepared through method 3 and using the platform for photopolymerization had a much higher bicarbonate exchange percentage.
Sample | Synthesis Method | CO2 Uptake at 20 Hours (µmol/g) | CO2 Uptake Kinetics (first 5 hours) (µmol/g*hr-1) | Bicarbonate Exchange (1 soak)
1% (w/w) DE Microspheres | method 3 + platform | 85.4 | 13.0 | 75.9%
Control | method 3 + platform | 57.3 | 6.6 | 75.9%
Control | method 1 + vial | 18.3 | 2.34 | 59.4%
1% (w/w) DU Microspheres | method 1 + vial | 13.2 | 1.1 | 50.0%

## Slide 26
Accomplishments & Acknowledgements
Accomplishments
Used this project for my research essay and was nominated by ASU for the Barry Goldwater Scholarship for undergraduate researchers in STEM (winners announced last Friday in March!)
Recently presented a non-technical version of this research at the Grand Challenges Scholars Program National Annual Network Meeting (relating to the “develop carbon sequestration methods” grand challenge)
Accepted to present this research at the national Stanford Research Conference in early April
Used this project experience in carbon capture/air quality to obtain a position at the Pacific Northwest National Laboratory this upcoming summer (project on aerosol characterization)
Acknowledgements
Special thanks to Dr. Green, Ani, Kacie, and Husain for mentorship, advice, and equipment operation.