## Slide 1: Investigation of Stress Concentrations in Parts Manufactured with Fused Deposition Modeling
Winona Roulston, Nathan Bleakley, and David B. Lanning
Embry-Riddle Aeronautical University – Prescott, Az
2024 Space Grant Symposium , 20 April 2024
Notes: General introduction slide

## Slide 2
Acknowledgements
Notes: General introduction slide

## Slide 3
Fused Deposition Modeling
Thermoplastic filament is heated to its melting temperature​
​
Extruded through the nozzle​
​
Deposited layer-by-layer
Notes: General introduction slide

## Slide 4
Parameter Variations
Notes: General introduction slide

## Slide 5
Traditional Solid Mechanic Theory
Notes: General introduction slide

## Slide 6
SATEC Machine Testing - High Density Grip Tab
High density infill “grip tab”
Prevents specimen crushing
Minimal impact on strength
Notes: General introduction slide

## Slide 7
Results From Prior Testing
Failure location deviates from predicted location
Notes: General introduction slide

## Slide 8
Nominal Stress at Failure
Notch
Hole
V - Notch
Ellipse
20%
Chart: kt
| 2.2000000000000002 | 2.4 | 2.5
20% | 1822.4987 | 1476.4564 | 1363.053
20% | 2637.2444 | 2061.267 | 1856.1853
20% | 1733.4285 | 1506.7427 | 1346.184
20% | 2998.3926 | 2030.7489 | 1974.3493
40% | 2497.9152 | 2283.7412 | 2033.0606
40% | 3435.05 | 2516.2911 | 2416.1814
40% | 2649.8962 | 2103.054 | 1867.2582
40% | 3430.0264 | 2588.0591 | 2424.4402
60% | 3314.2657 | 2963.7288 | 2835.587
60% | 3784.442 | 3374.2012 | 2964.4045
60% | 3583.0306 | 2650.5011 | 2074.8819
60% | 3597.7657 | 3001.2262 | 2636.8277
40%
60%
Notes: General introduction slide

## Slide 9
Theoretical Stress Concentration Factor
Chart: Notch
| 0.26981597239217114 | 0.20206655053714856 | 0.15150528042550773
20% | 1.1155 | 1.377 | 1.4918
40% | 1.3345 | 1.4597 | 1.6396
60% | 1.1725 | 1.3112 | 1.3704
Theory | 2.894 | 2.7283 | 2.5683 | 2.4142 | 2.2664 | 2.1251 | 1.9908 | 1.8636 | 1.7438 | 1.6319 | 1.528 | 1.4325 | 1.3457 | 1.2679 | 1.1994 | 1.1405 | 1.0915 | 1.0527
Chart: Hole
| 0.38769159159912697 | 0.26006204366082408 | 0.19510777292471496
20% | 0.76086 | 0.98522 | 1.0953
40% | 0.97044 | 1.3551 | 1.3797
60% | 1.0268 | 1.1516 | 1.3108
Theory | 2.86 | 2.7319 | 2.6185 | 2.519 | 2.4324 | 2.3576 | 2.2936 | 2.2395 | 2.1943 | 2.157 | 2.1266 | 2.1021 | 2.0825 | 2.0668 | 2.0541 | 2.0434 | 2.0336 | 2.0237 | 2.0129
away from hole | 0.76086 | 0.98522 | 1.0953 | 1.3551
Notes: General introduction slide

## Slide 10
Shell Stress
Extra shell area due to hole perimeters
Notes: General introduction slide

## Slide 11
Failure Locations
Specimen Infill Density
Reinforced Grip Tab
Notes: General introduction slide

## Slide 12
Phantom Camera Results
Notes: General introduction slide

## Slide 13
Damage in 3D Printed Specimens
Notes: General introduction slide

## Slide 14
Summary
Specimen strength increases with the higher infill densities​ and behaves more homogeneous
Traditional solid mechanics is not applicable in failure prediction​
Shell printing parameters may reinforce and shield against stress concentrations
Viscoelastic properties are experienced in the testing
Notes: General introduction slide

## Slide 15
References
Slide 2 Przekop, R. E., Gabriel, E., Pakuła, D., & Sztorch, B. (2023a, June 21). Liquid for fused deposition modeling technique (L-fdm)-a revolution in application chemicals to 3D printing technology: Color and elements. MDPI. https://www.mdpi.com/2076-3417/13/13/7393
Slide 9 Hill, Logan, Brown, Trey, Luchik, Tyler, and Lanning, David, “Investigation of infill pattern in Parts Manufactured with Fused Deposition Modeling” SAMPE 2022 Conference, Charlotte, NC.
Notes: General introduction slide