## Slide 1: 3D Printed Afterglow Filters for Air Pollution Control
Gabriel Negrao, Adnan Abdullahi, Mikiye Lamansky, Jean M. Andino
School for Engineering of Matter, Transport, & Energy at Arizona State University

## Slide 2: How does H2S form?
Bacteria decompose sulfates, creating hydrogen sulfide
SO2-4 + Organics → H2S + CO2
Unchecked high concentrations can cause severe irritation and death
H2S can be split, generating hydrogen
H2S + energy → H2 + S
Incredible potential for green energy
Photocatalysts can reduce the thermodynamic energy barrier
  How can the energy demand be further reduced?
H2S
Images generated with the assistance of AI
Image generated with the assistance of AI

## Slide 3: Opportunity
DIW structures adsorb H2S and split it when exposed to light
Afterglow reduces energy demand for photocatalytic reaction
Direct Ink Writing (DIW)

## Slide 4: Goal and Approach
Goal: Use DRIFTS to analyze the composition and behavior of H2S on these structures.
DRIFTS: Allows for structural analysis of solid samples
Prepare samples of printed filters and isolated components
Cross-reference DRIFTS readings to isolate unique features
  ZnS vs ZnS:Cu
  Filter material pre/post H2S exposure
Figure adapted from: https://www.swri.org/sites/default/files/brochures/drifts.pdf

## Slide 5: ZnS vs ZnS:Cu
Single peak at 1120 vs Split peaks at 1130-1040
Indicate copper substitution in ZnS matrix
Verified structurally significant doping of copper

## Slide 6: Filter Material Before/ After H2S Exposure
No features suggesting H2S on surface (2500-2625 cm-1)
Interesting behavior at 1655 cm-1, intensifying -OH peak?
Subtracted spectra to isolate novelties

## Slide 7: Filter Material Before/ After H2S Exposure
Intensifying peak shows formation of water after H2S exposure
  How did water get there?
  Where did the H2S go?
Potential reaction paths:
2 H2S + O2 → 2 S + 2 H2O
2 H2S + 3 O2 → 2 SO2 + 2 H2O
Could SO2 off-gas during reaction?
Solution: Develop a method to expose the filter to H2S in an enclosed reactor where DRIFTS can be taken immediately before and after exposure.
Negates oxidation, off-gassing, uneven material distribution

## Slide 8: Future Work
DRIFTS immediately pre/post H2S exposure in specialized reactor
Mass balances for the conversion of H2S on and over different filters materials
Collect further DRIFTS to analyze properties of afterglow phosphor

## Slide 9: Thank You!