## Slide 1: Examining Effects of Post-Processing Operations on Laser Powder Bed Fusion 3D Printed Parts
Molly Auer
Dr. Hannah Budinoff
University of Arizona
Arizona NASA Space Grant Consortium Student Research Symposium
SkySong, Arizona State University Scottsdale Innovation Center
April 19, 2025

## Slide 2
Introduction
2
Laser Powder Bed Fusion (LPBF)
Metal additive manufacturing 3D printing process
(Hendrixon, 2023)
Advantages | Disadvantages
Fabricate Complex Geometries | High Residual Stresses
Precisely Distribute Material | Significant Porosity
Compatible with Topology Optimized Parts | High Surface Roughness
Fast | Costly
Post processing operations, such as heat treatment, can mitigate these issues and enhance structural integrity
Reduce deformation
Relieve residual stresses
Improve material properties

## Slide 3
Objectives
3
Examine effects of post-processing operations on LPBF prints
Provide guidance on optimizing order of operations and processing parameters
  Minimize distortion and residual stresses
  Increase part manufacturability
Infer how post-processing decisions can increase LPBF manufacturability
(MakerVerse, 2024)
  Support Removal
  Heat Treatment
  Base Unbolting
  Base Removal
(Materialise, 2024)

## Slide 4
Simulated LPBF printing of 2 Topology Optimized Parts
Ansys Mechanical
Titanium alloy (TI-6Al-4V)
0.5 mm mesh
Generated supports and base plate
Methodology
4
Order | Operation | Simulation Parameters
1 | Base Unbolting | Instantaneous
2 | Base Removal | Directional, 0.5 mm Step Size, Cut at 0◦
3 | Support Removal | Instantaneous
4 | Heat Treatment | Anneal at 850◦C, Heat up 10 minutes, Hold 1 hour, Cooldown 1 hour
Part 1
32x32x32 mm
~100K elements
Part 2
25x32x28 mm
~130K elements

## Slide 5
Simulated 9 processes per part
Methodology
5
Process Number | Operations
1 | None
2 | Base Unbolting
3 | Base Unbolting, Heat Treatment
4 | Base Unbolting, Base Removal
5 | Base Unbolting, Base Removal, Heat Treatment
6 | Base Unbolting, Support Removal
7 | Base Unbolting, Support Removal, Heat Treatment
8 | Base Unbolting, Base Removal, Support Removal
9 | Base Unbolting, Base Removal, Support Removal, Heat Treatment

## Slide 6
Maximum Deformation Visualization for Part 1
Results
6
Build, Base Unbolting, Base Removal
Heat Treatment

## Slide 7
Maximum Residual Stress Visualization for Part 1
Results
7
Build, Base Unbolting, Base Removal
Heat Treatment

## Slide 8
Effects of Post Processing Operations
Heat Treatment increased distortion by 34% on average
Results
8
Chart: Part 1
| 1 | 2-3 | 4-5 | 6-7 | 8-9
Before Heat Treatment | 0.51667 | 0.43693 | 0.38765 | 0.44553 | 0.3837
After Heat Treatment | 0 | 0.76278 | 0.46315 | 0.57605 | 0.45997
Chart: Part 2
| 1 | 2-3 | 4-5 | 6-7 | 8-9
Before Heat Treatment | 0.38346 | 0.26859 | 0.68123 | 0.28265 | 0.68701
After Heat Treatment | 0 | 0.41 | 0.74244 | 0.39937 | 0.88055
Chart: Max Deformation
Part 1 | 0.51667 | 0.43693 | 0.76278 | 0.38765 | 0.46315 | 0.44553 | 0.57605 | 0.3837 | 0.45997
Part 2 | 0.38346 | 0.26859 | 0.41 | 0.68123 | 0.74244 | 0.28265 | 0.39937 | 0.68701 | 0.88055
Scattered Trends across parts and processes

## Slide 9
Results
9
Clear trend that processes involving heat treatment relieved residual stresses
Chart: Max Residual Stress
Part 1 | 1377.8 | 1382 | 477.97 | 1371.5 | 408.54 | 1395.8 | 400 | 1363.3 | 407.84
Part 2 | 1473.7 | 1345 | 445.65 | 1263.5 | 474.36 | 1337.3 | 487.07 | 1259.9 | 143.9
Chart: Part 1
| 1 | 2-3 | 4-5 | 6-7 | 8-9
Before Heat Treatment | 1377.8 | 1382 | 1371.5 | 1395.8 | 1363.3
After Heat Treatment | 0 | 477.97 | 408.54 | 400 | 407.84
Chart: Part 2
| 1 | 2-3 | 4-5 | 6-7 | 8-9
Before Heat Treatment | 1473.7 | 1345 | 1263.5 | 1337.3 | 1259.9
After Heat Treatment | 0 | 445.65 | 474.36 | 487.07 | 143.9
Effects of Post Processing Operations
Heat Treatment reduced residual stress by 70% on average

## Slide 10
Results and Conclusions
10
(Ansys Help, 2024)
To minimize distortion, heat treatment should be performed:
After Base Unbolting
Before Base and Support Removal
After Base and Support Removal
Ideal Order of Operations:
Base Unbolting
Heat Treatment
Base Removal
Support Removal
Heat Treatment

## Slide 11
Ideal Process Parameters
11
Heat Treatment:
Time
  Slow ramp and cooling time (5-10 ◦C/min) to prevent harmful thermal gradients and improve ductility
  Shorter hold times (0.5-2hr) for higher temperatures (800-1000◦C)
  Longer hold times (2-5hr) for lower temperatures (400-800◦C)
Temperature
  Lower temperatures (400-800◦C) to balance strength and ductility
  Higher temperatures (800-1000◦C) to increase toughness and strength
Base Removal:
Step Size
  Smaller step size (<0.5 mm) for smoother detachment, lower efficiency
  Larger step size (>0.5 mm) for coarser removal, higher efficiency
Direction
  0◦ for a smooth horizontal removal
  >0◦ for more aggressive material removal
    Ideal with support raft to prevent damaging part itself
(Laleh, 2023)
Results and Conclusions

## Slide 12
Future Studies
Different parts
Different materials
Different part sizes
Data after heat treatment (Ansys bug)
Advance Additive Manufacturing
Relativity Space’s 3D printed rocket
Future Implications
(Sheetz, 2020)
12

## Slide 13
Ansys Help. (2024). Simulating Heat Treatment after the Build.
  https://ansyshelp.ansys.com/account/secured?returnurl=/Views/Secured/corp/v241/en/add_ag/add_ag_adv_top_heat_treat.html
Hendrixson, S. (2023, July 26). What is Powder Bed Fusion 3D Printing? Gardner Business Media, Inc.
  https://www.additivemanufacturing.media/articles/am-101-powder-bed-fusion-pbf
Laleh, M., et al. (2023). Heat treatment for metal additive manufacturing. Progress in Materials Science.
  https://www.sciencedirect.com/science/article/pii/S0079642522001323
MakerVerse. (2024, October 16). Laser Powder Bed Fusion (LPBF). MakerVerse.
  https://www.makerverse.com/offering/laser-powder-bed-fusion-lpbf/
Materialise. (2024, November 14). 5 easy ways to remove metal support structures.
https://www.materialise.com/en/inspiration/articles/5-ways-to-remove-metal-support-structures
Sheetz, M. (2020, October 8). Inside Relativity Space’s 3D-printing rocket “factory of the future.” CNBC.
  https://www.cnbc.com/2020/10/07/inside-relativity-space-hq-3d-printer-rocket-factory-of-the-future.html
References
13

## Slide 14
Special thanks to:
Dr. Hannah Budinoff, Principal Investigator and Mentor
Juan Machado Jr, Intern Advisor
Nathan Hertlein, Project Advisor
Arizona NASA Space Grant
Air Force Research Laboratory
University of Arizona, Systems and Industrial Engineering
Manufacturing and Design Exploration Lab: https://sites.arizona.edu/made-lab/
Acknowledgements
14
This material is based on research sponsored by the Air Force Research Laboratory under agreement number FA8650-20-2-5853. The U.S. Government is authorized to reproduce and distribute reprints for Governmental purposes notwithstanding any copyright notation thereon. The views and conclusions contained herein are those of the authors and should not be interpreted as necessarily representing the official policies or endorsements, either expressed or implied, of the Air Force Research Laboratory or the U.S. Government.

## Slide 15
Thank you!