## Slide 1
Mentor: Dr. Brandon Chalifoux, Lightweight Optics Lab, Wyant College of Optical Sciences
Arizona NASA Space Grant Symposium, 19 April 2025
Selective Laser Etching of Slumped Mirrors for X-Ray Astronomy
Dillan Synan
Notes: name, year
Project name

## Slide 2
Purpose:
  The current NASA flagship X-ray space telescope, Chandra, is 26 years old
  My research group has been tasked with developing technology for next generation X-ray optics
Nasa.gov
Notes: In case you don’t know, there is a space telescope that images x ray data
The wider purpose of my project is:

## Slide 3
Background:
X-Ray optics are challenging
  Since the wavelength of X-rays are so small, lenses cannot be used and imperfections on the order of an X-ray prevent reflection
  All X-ray telescopes are mirror-based, precise, and in space
  One approach is to use a collection of small mirrors where incident x-rays just barely graze the mirror surface
Nasa.gov
Notes: So a little bit about x –rays:
X-rays are really small, which creates a lot of unique challenges
…
So how do you make the optics for an X-ray space telescope?

## Slide 4
Objective: Find a way to write and etch Flex (Mirror) Segment pattern into curved substrate
Chalifoux, APRA 2025
25 mm
Flat Flex Segment after laser writing process, before chemical etching
Notes: So, what really is my project?
Explain that writing onto curved substrates wasn’t a capability of the laser system

## Slide 5
Background:
Slumping
Writing,
etching
Backside coating
Spacer fabrication
Frontside coating
Base fabrication
Welding
Alignment & figuring
X-ray testing
Repeat for all shells
Iterate to convergence
Flex Segment
Flex Module
Oversized segment
Flex Segment fabrication
Coatings
Assembly
Chalifoux, APRA 2025
Notes: Now, a brief overview of the whole process of making these mirrors:
…

## Slide 6
Background:
6
Isolation flexure
X-rays in
X-rays out
Secondary mirrors
Primary mirrors
Flex Segment
50 mm × 50 mm × 0.5 mm
Optical surface
Concave side
Realignment beam
Flex Segments welded to spacers
Anatomy of a Flex Module
6
6
Cross section of X-ray mirror system
Sci.esa.int
Notes: Now, we take a closer look at one unit of the mirror system (a flex module)
…

## Slide 7
Background:
Selective Laser Etching:
Femtika.com
Notes: So, how exactly, do you write a fabricate a part using a laser?
…

## Slide 8
Objective: Find a way to write and etch Flex Segment pattern into curved substrate
    Accomplishments:
    Learned how to operate the laser system
    Developed workflow to write machine code from desired geometry
    Wrote 3D curved patterns into a flat substrate
    Wrote 3D curved patterns into a curved substrate
    Etched physical product
Notes: Now that we know a lot more about the purpose of the project, what was the goal, and what did I actually do?
…

## Slide 9
Workflow:
Design part, export as 2D DXF file. SOLIDWORKS
Scan part surface. Chromatic Confocal Sensor
Interpret 2D DXF output, adds laser commands. CADFusion
Produce 2D laser program (text file). Custom Lab Software
Output surface data. Custom Lab Software
Interpolate 2D laser program onto surface data. My Custom Software
Write new 3D pattern using modified text file. Laser System
Notes: So to visualize the process I landed on:

## Slide 10
Beam conditioning
Ultrafast Laser
Beam focusing, imaging, on-machine metrology, and workpiece stage/ chuck
Workpiece
Equipment:
Translation Stage, Moves in xy Plane
Linear Translation Stage, Moves in z
x
y
z
Laser parameters:
1.2 μJ pulse energy
52 kHz repetition rate
3 ps pulse duration
500 nm pulse pitch
Write speed: 25 mm/s
Layer spacing: 5 μm
Circular polarization
Substrate glass:
Schott Borofloat 33
Chalifoux, APRA 2025
Chromatic confocal sensor not shown
Notes: So once you’re in the lab and ready to make your part, how does this work?
The laser is on one side, and its light has to be directed and manipulated in many ways before it is used.
Special type of laser, an ultrafast laser.
Explain motion
Explain how to do process:
Clean and mount slumped substrate onto a workpiece
Perform surface scan using a tool called the chromatic confocal scanner
Run my code using scan data and part data
Confirm that the file and graph I wrote makes sense
Enclose laser system and run

## Slide 11
Results:
Notes: AND, I was successful!

## Slide 12
Acknowledgments:
My PI and Space Grant mentor, Dr. Chalifoux
Research Engineer Ian Arnold
Arizona Space Grant

## Slide 13
Thank You!

## Slide 14
Citations
  https://femtika.com/process/selective-laser-etching/ for SLE GIF
  RTF kickoff 2024, Brandon Chalifoux
  NASA APRA Proposal
  Em spectrum: https://mynasadata.larc.nasa.gov/basic-page/electromagnetic-spectrum-diagram

## Slide 15
Interpolating Flex Segment onto Substrate:
Notes: Skipping over many details, the process can be visualized as such:
Design flex segment, turn lines into many points because each point must eventually have an associated z coordinate
While in the lab, use position scan data from substrate surface to write machine code for slumped flex segment
Also graph it to make sure you’re writing what you should be writing
As for the system that I use to modify these slumped mirrors:

## Slide 16
Approximation of curves as small line segments:
1mm radius curve split into 5 line segments, 8.6 micron sag, compensated by VELOCITY ON
20x zoom
40x zoom