## Slide 1
ASU/NASA Space Grant Program
Optimized Catalyst Preparation for Polymer Electrolyte Membrane Fuel Cells
Anthony Adame
Advised by: Dr. A.M. Kannan

## Slide 2: Polymer Electrolyte Membrane Fuel Cell
ASU/NASA Space Grant Program
[1] Polymer Electrolyte Membrane Fuel Cell

## Slide 3: Uses of Fuel Cell
ASU/NASA Space Grant Program
Automobiles
Grid Power
  Homes
  Hospitals
  Hotels
Telecommunications
Water Treatment Plants
[2] GM Fuel Cell Equinox

## Slide 4: Fuel Cell Challenges
ASU/NASA Space Grant Program
Cost
  Platinum (Pt)
  Hydrogen
Durability
  Degradation of Pt
  Degradation of GDL
Performance
[3] GM Fuel Cell Equinox Ghost Figure

## Slide 5: Two – Phase Transfer Method ( Dr. A.M Kannan and J.F. Lin of Arizona State University)
ASU/NASA Space Grant Program
[4] Two-Phase Transfer Method courtesy of Dr. A.M Kannan and J.F. Lin

## Slide 6: Project Goals
ASU/NASA Space Grant Program
Determine optimum sintering temperature of catalyst material
Determine optimum molar ratio of citric acid used to treat multi-walled carbon nanotubes (MWCNTs)
Determine optimum molar ratio of dodecanethiol (DDT) to Pt used to prepare catalyst material

## Slide 7: Experiments Conducted
ASU/NASA Space Grant Program
Experiments 1-3
Sintering Temperature ( ° C ) (1.6 mMol citric acid, 8: 1 DDT ratio)
300
500
800
Experiments 3-5
Citric acid concentration (mMol) (8:1 DDT ratio, 800 °C sinter temp. )
1.6
0
3.2
Experiments 6 - 8
Molar Ratio of DDT to Pt (1.6 mMol citric acid, 800 °C sinter)
1: 1
2: 1
8: 1

## Slide 8: Performance Data – Sintering Temperature
ASU/NASA Space Grant Program
[5] Performance data of sintering temperature experimentation

## Slide 9: Performance Data – Citric Acid Concentration
ASU/NASA Space Grant Program
[5] Performance data of citric acid concentration experimentation

## Slide 10: Performance Data – DDT to Pt Ratio
ASU/NASA Space Grant Program
[5] Performance data of DDT to Pt Ratio experimentation

## Slide 11: Results
ASU/NASA Space Grant Program
800° C is optimum sintering temperature for MWCNT supported catalyst material
  Removes all thiol material  reduces resistance
Citric acid concentration of 1.6 mmol is optimum acid concentration for
functionalizing of MWCNTs
  Lesser concentration does not form as many functionalized OH groups
  Higher concentration damages MWCNT structure and degrades nanotubes into carbon material
DDT to Pt ratio of 8: 1 is the optimum ratio for MWCNT supported catalyst
material

## Slide 12: Outcomes
ASU/NASA Space Grant Program
Project
Experimentation and Results Published – Journal of Electrochemical Society –
Accepted
New experimentation and results being conducted for future publication
Personal
Learned creative ways of thinking, how to conduct experiments, how to publish literature, and other priceless lessons from Jay Lin, my graduate mentor
Learned the importance of fuel cell technology and will conduct graduate research
on fuel cell technology under the advising of Dr. A.M. Kannan

## Slide 13: Acknowledgements
ASU/NASA Space Grant Program
I would like to thank the following for their help and support throughout my experience with the AZ /NASA Space Grant Program:
Dr. A.M Kannan (Mentor)
Jay Lin (Graduate Mentor)
Chad Mason (Co-worker)
Rashida Villacorta
All fuel cell lab colleagues
Tom Sharp
Candace Jackson
Danielle Pies
Meg Hufford
AZ / NASA Space Grant
Arizona State University – Polytechnic Campus
University of Arizona

## Slide 14: References
ASU/NASA Space Grant Program
[1] ] J.Hules and U. Wang, “ Scientists discover why the right amount of moisture in the membrane plays a key role in fuel cell efficiency,” in National Energy Research Scientific Computing Center, [online].
Available: http://www.nersc.gov/news/science/sandwich.php ]. Accessed: [Apr 12, 2010].
[2] National Hydrogen Association, “General Motors Equinox fuel cell,” Hydrogenassociation.org,
[online]. Available: http://www.hydrogenassociation.org/media/mediaDownload.asp
[Accessed: April 12, 2010].
[3] C. and S. Gable, “Chevrolet Equinox Fuel Cell Vehicle test drive,” About.com, [online].
Available: http://alternativefuels.about.com/od/fuelcellvehiclereviews/fr/equinoxfuelcell.htm,
[Accessed Apr. 12, 2010].

## Slide 15: References
ASU/NASA Space Grant Program
[4] J.F. Lin, “Nano-Enabled Catalyst for High Power Proton Exchange Membrane Fuel Cells (PEMFCs),”
Thesis Presentation, Arizona State University, Apr. 4, 2010.
[5] J.F. Lin, A. Adame, and A.M. Kannan, “Development of durable platinum nanocatalyst on
carbon nanotubes for proton exchange membrane fuel cells,” in Journal of
Electrochemical Society - Accepted.