## Slide 1: Development of Heavily Aluminized Solid Rocket Propellant
Ruby Gomez (Presenter)
Gaines Gibson

## Slide 2: Outline
Daedalus Astronautics at ASU
Project Purpose
Chemical Properties
Mixing Procedures
Testing Equipment
Testing Results and Analysis

## Slide 3: Daedalus Astronautics
Student Organization at Arizona State University
Extensive Propulsion Experience
Community involvement

## Slide 4: Project Purpose
To develop a heavily aluminized solid rocket propellant
To characterize the new propellant
“Characterize” in using rocket design equations, simulation, and empirical testing on the new solid propellant
To test propellant on conventional (delavel) and multi-grid nozzle
funded project

## Slide 5: Chemical Properties
Liquids
HTPB (Hydroxyl-terminated-polybutadiene) similar color to wax paper, highly viscous, and a binder (to bind the fuel (aluminum) and oxidizer (ammonium perchlorate))
DOA (Dioctyl Adipate) - light colored oil used as plasticizer (to reduce viscosity of propellant)

## Slide 6: Chemical Properties
Liquids
Castor oil – very pale yellow liquid used to harden the grains, to prevent fractures and increase the density
Tepanol – is a very sticky substance used as a bonding agent to strengthen the bond between the binder (HTPB) and oxidizer (ammonium perchlorate)
Isonate 143L – is the curative which starts the processing of hardening the solid propellant
Curing Agent

## Slide 7: Chemical Properties
Fuel
Aluminum – used as a fuel in powder form 325 mesh
Oxidizer
Ammonium Perchlorate – is the oxidizer

## Slide 8: Chemical Properties
Solids
Carbon black – a dyeing agent , prevents the grains from breaking down due to the ultraviolet light released during combustion
Ferric (Iron III) oxide - creates thermite reaction, serves as a catalyst to the combustion reaction

## Slide 9: Chemical Properties
Solids
Strontium chromate – very powerful oxidizer
Copper II oxide- creates thermite reaction, serves as a catalyst to the combustion reaction

## Slide 10: Mixing Procedures
Liquids – HTPB, DOA, CO, TP
Fuel – aluminum
Vacuum
Solids – CB, FO, SC, C3O
Oxidizer – ammonium perchlorate
Curing Agent – Isonate 143L
Cast
Heat Treatment
Custom made Vacuum plate
Custom made Heat Box
Kitchen Aid mixture

## Slide 11: Raytheon Propellant Formulation
Order | Material | Purpose / Component | Percentage | Calculated Weight (lb)
1 | HTPB | Binder | 8.5 | 0.64425
2 | Aluminum | Fuel | 19 | 1.425
3 | DOA | Plasticizer | 2 | 0.15
4 | HX-752 | Bonding Agent | 0.3 | 0.0225
5 | Tepanol | Bonding Agent | 0.5 | 0.0375
6 | Ammonium Perchlorate (AP) | Oxidizer | 69 | 5.175
7 | IPDI | Curative | 0.59 | 0.04425
N/A | TPB | N/A | 0.02 | -

## Slide 12: Daedalus Propellant
 | Original CrazyPants3 Formulation | CrazyPants3 Modification 1 | CrazyPants3 Modification 2
Chemical | Percentage | Percentage | Percentage
Ammonium Perchlorate (200 micron) | 73.8 | 72.3 | 70.96
HTPB | 14.2 | 13.9 | 13.65
Aluminum (325 mesh) | 5 | 7 | 9
Dioctyl Adipate | 3.55 | 3.48 | 3.41
Isonate 143L | 1.84 | 1.80 | 1.77
Iron Oxide | 0.55 | 0.54 | 0.529
Strontium Chromate | 0.30 | 0.29 | 0.288
Carbon Black | 0.20 | 0.196 | 0.192
Tepanol | 0.20 | 0.196 | 0.192
Castor Oil | 0.20 | 0.196 | 0.192
Copper Oxide | 0.15 | 0.147 | 0.144
Silicon Oil | 0.01 | 0.009 | 0.009

## Slide 13: Mixing Difficulties
Tepanol and Ammonium production
Texture of Heavily Aluminize Propellant
Hardening
Custom built casting rack
Casted grain

## Slide 14: Testing Equipment

## Slide 15: Testing Equipment
Data Acquisition (DAQ) model 718B – records pressure and thrust data
Test Stand – custom built test stand

## Slide 16: Test One
Test one failure analysis
Root cause analysis found failure due to nozzle throat area
Extremely aggressive propellant burn
Summary
Original CP-3 Propellant
Result: Catastrophic over-pressurization

## Slide 17: Test Two
Test two failure analysis
Root cause was extremely fast regression rate
Exact same hoop stress failure as first test
Summary
7% CP-3 Propellant
Result: Catastrophic over-pressurization
60 lb thrust at operating pressure

## Slide 18: Special Thanks
Matt Summers

## Slide 19: Questions