## Slide 1: Effects of Swirl Injector Design on Hybrid Rocket Fuel Regression Rate (Grain Development)
Team Members: Raul Lugo, Kyle Bowerman
Mentor: Matthew Summers

## Slide 2: Research Overview
Background
  Hybrid Rocket Propulsion
  Swirl Injectors
  Regression Rate
Grain Development
  Sizing
  Formulation
  Mixing and Casting

## Slide 3: Background: Hybrid Rocket Propulsion
Propellant in solid and liquid phases
Fuel type: Hydroxyl-terminated polybutadiene (HTPB) in solid state
Oxidizer type: Nitrous oxide (N2O) in liquid state
Precombustion chamber
  Where atomization occurs
Postcombustion chamber
  For proper combustion

## Slide 4: Background: Swirl Injectors
Create a central toroidal recirculation zone (CTRZ)
  Improves regression rate
  Creates stable combustion
Classification
  S = Swirl number
  Φ = Swirl angle

## Slide 5: Background: Regression Rate
Regression rate is the amount of solid hybrid fuel that is receding from the surface during combustion along the length of the cylindrical grain.

## Slide 6: Grain Development: Sizing
L = length of grain
N = number of ports
mf = fuel mass flow rate
Ri = Initial
ρf = fuel density
r = regression rate
O/F = oxidizer to fuel ratio
Isp = specific impulse

## Slide 7: Grain Development: Sizing
O/F | 8
a | 0.1296
n | 0.778
r_dot | 0.0283 (m/s)
m_ox | 0.25 (lb/s)
m_f | 0.0313 (lb/s)
ρHTPB | 0.0336 (lb/in3)
I.D. | 1.5 (in)
O.D. | 2.25 (in)
L | 7 (in)
2.25 in
1.5 in
7 in

## Slide 8: Grain Development: Formulation
Liquid HTPB = Fuel
Isonate 143L = Curative
Silicon Oil = Lubricant
Carbon Black = Opacity
Amount | Chemical/Additive
85% | HTPB
15% | Isonate 143L
2 teaspoons | Carbon Black
N/A | Silicon Oil

## Slide 9: Grain Development: Mixing and Casting
Mixing of formulation
  Used a Kitchen Aid stand mixer
Vacuuming
  To ensure no air pockets when pouring into cast
Vacuum Pump
Mixing Bowl
Relief Valve
Polycarbonate Sheet

## Slide 10: Grain Development: Mixing and Casting
Mylar sheet coated with mold release
24 hour curing process
Heat box heated from 100–140 degrees F
Casting rod
Heat box
Cured grain
Mylar
Phenolic liner

## Slide 11: Future Plans
Develop multiple grains for multiple fire tests in a day
Improve grain development process
  Mix and cast multiple grains at once
  Improving time for development
Regression rate analysis of aluminum addition in formulation
Analysis of other fuel grains ex. paraffin

## Slide 12: Acknowledgements
ASU/NASA Space Grant Consortium
Raytheon Company
Matthew Summers (Mentor)

## Slide 13: Thank you. Any Questions or Comments?