## Slide 1: Composite Material with Structural and Power Storage Capabilities
Chris Simpson

## Slide 2: Introduction
Electrical circuit board with capacitors:
Capacitors – electricity storage devices that can charge and discharge instantaneously.
Basic layout of dielectric capacitor:
Photo courtesy of circuitelectronics.info
Photo courtesy of wikipedia.org

## Slide 3: Capacitance
Capacitance can be calculated by:
2 ways to increase capacitance:
- minimizing the separation distance
- maximizing the surface area
 Permittivity C  Capacitance (Farads)
 Electric constant  Current (Amps)
 Surface area (m2) (  Rate of change in voltage (V/s)
 Separation distance (m)

## Slide 4: Introduction
Electric Double Layer Capacitors (EDLCs)
- EDLCs use an electrolyte solution with a separator.
- Solid Polymer Electrolyte (SPE) add structual
integrity and allow ion conductivity for high
capacitance

## Slide 5: Purpose
Purpose:
Develop EDLCs with structural emphasis
Applications:
Structurally integrated into:
- the body of vehicles
- the skin of aircrafts
- the walls of buildings
- the casings of electronics

## Slide 6: Application

## Slide 7: Composite EDLC Layout
Carbon fiber electrode
  Lamina
Separator
  Lamina
Solid Polymer Electrolyte (SPE)
  Matrix
Copper current collectors

## Slide 8: Fabrication
Picture frame mold layout
Mold with finished capacitors
Oven press

## Slide 9: Electrical Testing
Measurement process – cyclic voltametry:
- Induce a charge across capacitor
- Measure capacitance, leakage resistance
Capacitors are tested using a function generator and a digital multimeter (DMM).
Measuring equipment

## Slide 10: Mechanical Testing
Tension testing (ASTM 3039)
Flexure Testing (ASTM 790)
Grips
3501 Celgard sample
2500

## Slide 11: Mechanical Testing Results
Tensile tests
Flexural tests
Li salt concentration does not
have a significant effect on strength.
Composite super-capacitors have strength and stiffness of the same order of magnitude as standard composite materials.

## Slide 12: Future Work
  Research more solid polymer electrolyte formulations to enhance specific capacitance
  as well as mechanical strength.
  Experiment with other composite materials

## Slide 13: Conclusions
Capacitors with structural capability are feasible.
High energy density is achievable.
The structural properties of the capacitors are comparable with those of regular carbon fiber materials.

## Slide 14: Acknowledgements
Thank you to:
NASA/NAU Space Grant
Dr. Barlow
Kathleen Stigmon
Dr. Ciocanel