## Slide 1: Characterization of Diffusion from Mesoporous Silica Nanoparticles for Potential Drug-Delivery Applications
Kate Li
Chemical Engineering & Biochemistry

## Slide 2: Mesoporous Silica Nanoparticles
Figure 1: Diagram of different ways to functionalize a mesoporous silica nanoparticle – external and pore surface functionalization (Colila et. al 2013).

## Slide 3: Why MSNPs?
Tunable drug delivery
  Antibodies for site specificity
  Within threshold size for cellular uptake (D ~100 nm)
  Controlled and sustained release
Applications: chemo toxic drugs, nonpolar with low bioactivity in the body due to poor solubility
Silica is bioinert
Glass cardiovascular system sculpture by Gary Farlow

## Slide 4: Modified Stӧber Process
Reagents:
  Cetyltetra-ammoniumbutylate (CTAB)
  Tetraethyl orthosilicate (TEOS)
  NaOH
  EtOH
  Water

## Slide 5: Forming a Liquid Crystal

## Slide 6: Experimental Procedure
Materials:
- TEOS (tetra ethyl orthosilicate)
- EtOH (ethanol)
- CTAB (cetyl trimethylammonium bromide)
- NaOH (sodium hydroxide)
- dI H2O(deionized water)
Characterization:
- N2 absorption
- SEM, TEM, SAXRD
Procedure:
Add .375 g of CTAB, .4375 mL 2.0 M NaOH and 30 mL dI H2O to roundbottom flask with magnetic stir bar and heat to 80⁰C for 30 minutes.
To clear solution, add 2.48 mL TEOS via rapid injection.
White precipitate will be observed after 1-2 minutes of stirring.
Maintain reaction temperature at 80⁰C for 2 hrs.
Isolate product via ethanol wash and centrifugation/sonication cycles of 10 minutes each, four times. Dilute and suspend in ethanol.

## Slide 7: Experimental Observations

## Slide 8: Results

## Slide 9: Results

## Slide 10: Theoretical Modeling

## Slide 11: Further research
Further research on the parameters of the Modified Stӧber Process
Attempting functionalization of surface and pores
Generate diffusion data

## Slide 12: Questions?
Thank you
NASA Space Grant
UA Honors College – Alumni Travel Grants
Dr. Anthony Muscat
NASA Space Grant Consortium