## Slide 1: Characterization of Lysine on the Surface of SiO2 Nanoparticles
Tom Osborn Popp
Arizona State University
Mentor: Jeff Yarger

## Slide 2: Introduction
Nanotechnology is an exciting field with applications in science, medicine, engineering and everyday life.
The field of nanomaterials is focused on development and manipulation of matter in the 1-100nm scale.
At the nano scale, quantum effects and surface interactions become very important

## Slide 3
Bulk
Nanoscale
Properties governed by surface interactions

## Slide 4: Motivations for the Study
How do molecules adsorb to silica surfaces? What functional groups play key roles in the adsorption process?
Nanoscale silica is a major subject of research in developments for drug delivery—silica is biocompatible. Drug adsorption to silica for controlled release.
Photo by Dr. Karen Wetmore
Intricate silica structures made by diatoms

## Slide 5: Goals of the Study
How does the amino acid lysine adsorb to the surface of silica?
In what orientation and with which functional groups does lysine preferentially adsorb to the surface?
Use Raman spectroscopy and both solution-state and solid- state NMR spectroscopy

## Slide 6: SiO2 Nanoparticles
SiO2
7.56 nm
Grid
SiO2
7.56 nm
Grid
SiO2
7.56 nm
Grid
Made by heating a solution of lysine in water mixed with solid silicon powder in suspension.
Freeze-dry solution to obtain solid product
TEM imaging shows average diameter of 7.56 nm

## Slide 7: Raman Spectroscopy

## Slide 8: 13C Solid State CP-MAS NMR
Lysine
Lysine adsorbed to SiO2-NP’s

## Slide 9: 1H Solution State NMR
Lysine
Lysine adsorbed to SiO2-NP’s

## Slide 10: Conclusions and Future Directions
In the solid state, lysine adsorbs via the side chain amine, possibly also at the alpha-amine.
In solution state, adsorption via the side chain amine.
To support these results, future NMR studies looking at amine chemical shifts of 15N using 15N-labeled lysine, and temperature studies to see a possible temperature dependence of orientation in the solution state
Control with experimental conditions how lysine adsorbs to the silica surface