## Slide 1: High-Temperature Corrosion in CSP Systems
Payton Meade, Chemical engineering
a.m. Kannan, department of engineering, CTI
Arizona state university

## Slide 2: What is CSP?
Concentrating Solar Power (CSP)
Not the same as the popular photovoltaic systems
  Can produce energy after the sun goes down
Uses a field of mirrors to concentrate light to a point
Department of Energy (DOE) is currently funding the construction of many around the Southwest

## Slide 3: Various CSP Power Towers
[1], [2] Photos courtesy of: SolarReserve
Notes: Crescent Dune Right/Ivanpah Left. Ivanpah is low impact. Uses 170K heliostats. Powers 140K Homes in S. Cal.

## Slide 4: How It Works
Field of sun-tracking mirrors (heliostats) focus the light to a point on a receiver tower
  Can track sun during summer and winter, when sun is at different angles to horizon
  Temperatures over 1000 oC
Salt at top of receiver is heated
  Acts as a heat transfer fluid (HTF)
    Carries energy and transfers to water
    Property of HTFs: low melt point
[3] Photo courtesy of: inhabitat.com
Notes: Explain what HTF is: carries energy and transfers to water (steam generator)
Properties of HTF (low melting point, stabile at high temps 1000, low corrosion piping)

## Slide 5: How It Works (cont.)
Heated salt goes through heat exchanger to produce steam
  Some of the heated salt is sent to a storage tank– produces energy after the sun goes down
Steam turbine generates electricity
  Most recent plants built can produce
    400 MWe (~140K homes) during peak periods [Ivanpah]
    110 MWe (~75K homes) [Crescent Dunes]
Notes: Ivanpah is largest in world with 3 power towers and 5 acres worth of heliostats
Crescent Dunes has one power tower

## Slide 6: Schematic of a CSP System
[4] Photo courtesy of: ASU Polytechnic, CTI

## Slide 7: Types of Heat Transfer Fluids
Nitrates currently used in CSP systems
Solar Salt is the specific mixture used in commercial CSP
  40 wt% KNO3 and 60 wt% NaNO3
  Eutectic mixture (lowest melting point)
  Melting point: <200 oC
  Stays stabile up to ~550-600 oC
First tested with Solar Two in the 1990s
Plants that use Solar Salt include Gemasolar and Crescent Dunes
Notes: Eutectic—if the composition is changed at all, then the melting point will drastically change

## Slide 8: Improving HTFs
New salts developed to combat previous problems
Combat freezing issues in pipes
  Hitec Salt: tertiary mixture
  7:53:40 wt% NaNO3:KNO3:NaNO2
  Lowered melting point: 142 oC
Lowered melting point also means it does not stay as stabile at high temperatures
  Stabile up to ~530 oC

## Slide 9: Objective
Study different salt compositions that could be used in CSP systems
  Melting point under 250 oC
  Stabile at temperatures above 800 oC
  Low corrosion of SS and Nickel alloys
  Costs less than $1/kg of salt

## Slide 10: A New Molten Salt: Current Work
Multidisciplinary University Research Initiative (MURI)
  ASU Polytechnic, Georgia Tech, University of Arizona
  Funded by DOE under SunShot initiative
    Reduce total installation costs of solar power by 2020
    Goal of $0.06/kWh
New salt composed of NaCl, KCl, and ZnCl2
  Chlorides stabile at high temperatures and low in cost
  Highly corrosive and high melting temperature

## Slide 11: Corrosion Mechanism
Notes: Destruction of metals by electrochemical reactions with the environment
Pulls moisture from air in case of chloride
Chloride more corrosive—more electronegative. It ionizes the metal more quickly, causes metals to react with water.

## Slide 12: Corrosion Data Techniques
Argon Gas Cylinder
Advanced Electrochemical System
Furnace
log | I | vs E plot
482
Thermocouple
log | I | →
- ←E→ +

## Slide 13: Results from Tafel Technique
CR (µm/year) = K1 [icorr.EW/ρ]
K1= known constant, EW= equivalent weight of metal, ρ= density of metal

## Slide 14: Findings
Corrosion of Hastelloy C-276 at 250 oC is ~10 µm/yr
  Increases as temperature goes up
    Due to Chlorine being more activated
Corrosion at 500 oC is ~40 µm/yr
Corrosion at 800 oC is over µm/yr
  Nitrates under 10 µm/yr, need to replace nitrates
Need to reduce in order to be commercially feasible!

## Slide 15: Corrosion Inhibitors
Nickel is ionized by Chloride and an oxidation/reduction reaction occurs spontaneously, corroding the metal
With an additive, the sacrificial metal is included in the O/R rxn, rather than the piping material

## Slide 16: Example of Galvanized Steel
Zinc coating on piping causes a thin oxide layer to form, preventing corrosion
  Passivation Layer
Cannot coat piping
  Too hot
  Additive to salt

## Slide 17: Continuing Work
Continue studies of the material in different temperatures/settings
  Inert setting/temps up to 1000 oC
Continue to study additives to reduce corrosion
  Test different metals like Mg, Zn, and Al

## Slide 18: Questions?