## Slide 1: Increasing Light Absorption in Concentrating Photovoltaic System Through Use of Anti- Reflective Sol-gel Coated Ball Lens
Safatul Islam
Mentor: Roger Angel
Steward Observatory Solar Lab

## Slide 2: Introduction
http://www.nasa.gov

## Slide 3: Concentrated Photovoltaics
Solar tracker system with paraboloidal mirrors concentrate onto focal point
  1000x suns
Light energy is transformed to electricity

## Slide 4: Power Conversion Unit
800 W module
  Ultimately sell for less than $1 per watt

## Slide 5: Power Conversion Unit

## Slide 6: Ball Lens

## Slide 7: Objectives
Need for Anti-Reflective coating
  Sol-gel
Overcoming spherical geometry
How can a thin film of Sol-gel be successfully coated onto a spherical ball lens?

## Slide 8: Methods
Spin coating application
Set up of necessary equipment

## Slide 9: Humidity controlled glovebox environment

## Slide 10: PID Controller to control spin rate

## Slide 11: Syringe and filter for deposition

## Slide 12: Table top furnace to fire coating

## Slide 13: Variables Affecting Film Coating
Smoothness of ball surface
  Polishing
Cleanliness of ball surface
  Sonicating, organic solvents
Structural Support
Sol-gel filtration
Syringe Application
Spin Rate

## Slide 14: Transmission Testing

## Slide 15: Results
From qualitative tests, coating was uniform throughout most of the ball
  Thinner at poles
Small area around the equator remained uncoated
Coating becomes thinner after firing
Few defects were noticeable
The coating functioned as desired

## Slide 16: Results

## Slide 18: Acknowledgements
Steward Observatory Solar Lab
  Dr. Roger Angel
  Dr. Thomas Stalcup
  Blake Coughenour
  Brian Wheelwright
  Andrew Geary
UA/NASA Space Grant Program
  Susan Brew

## Slide 19: Extra Slides

## Slide 20: Future Considerations
Eliminate some of the defects
  Automated cleaning and depositing apparatus
  Better support to hold and transfer ball lens
Other methods of coating
  Vacuum sputtering

## Slide 21: PCU Results

## Slide 22: Sol-gel
http://www.centexbel.be