## Slide 1: Bio-Inspired Cementation of Soil Using Plant Enzyme
Michael Bull3, Nasser Hamdan1, Jeffery Fijalka2,and Sean O’Donnell1
Research Supervisor: Professor Edward Kavazanjian, Jr.
1Graduate Research Assistant , 2 Graduate Laboratory Assistant, 3Undergraduate Researcher
ASU/NASA Space Grant Program
School for Engineering of Matter, Transport, and Energy; School of Sustainable Engineering and the Built Environment
Ira A. Fulton Schools of Engineering

## Slide 2: Outline
Cementation challenges & mitigations
What is bio-inspired cementation
Benefits of bio-inspired cementation
Cementation chemistry & mechanisms
Results
Recommendations for future work
ASU/NASA Space Grant Program
School for Engineering of Matter, Transport, and Energy; School of Sustainable Engineering and the Built Environment
Ira A. Fulton Schools of Engineering

## Slide 3: Cementation Challenges
Cemented mineral aggregate (e.g. concrete) is one of the most common construction materials today
Portland cement, the active binder in most concrete, is expensive & energy/CO2 intensive
The global supply of
Portland cement is
stressed
ASU/NASA Space Grant Program
School for Engineering of Matter, Transport, and Energy; School of Sustainable Engineering and the Built Environment
Ira A. Fulton Schools of Engineering
World and Chinese Cement Consumption Trend 1990-2006 (Global Cement Report, 2007)
Global CCS Institute

## Slide 4: Mitigation Measures
Increased efficiency of cement kilns & use of alternative kiln fuels and carbon sequestration
Use of supplementary cementitious materials such as blast-furnace slag & fly ash
Alternative cementation processes, including enzyme and microbial induced cementation
ASU/NASA Space Grant Program
School for Engineering of Matter, Transport, and Energy; School of Sustainable Engineering and the Built Environment
Ira A. Fulton Schools of Engineering
Fly Ash Bricks
Radco Buildtech Pvt Ltd
Microbially Cemented Brick
Ginger Krieg Dosier

## Slide 5: Enzyme Induced Cementation
Carbonate precipitation via hydrolysis of urea is a potentially inexpensive cementation method
Uses common materials (CaCl2, urea) & the enzyme urease
Requires less energy and processing steps than Portland cement
Plant derived urease is renewable & biodegradable
Smaller CO2 footprint than cement
ASU/NASA Space Grant Program
School for Engineering of Matter, Transport, and Energy; School of Sustainable Engineering and the Built Environment
Ira A. Fulton Schools of Engineering
Jackbean
Wikimedia commons

## Slide 6: Enzyme Induced Cementation via Hydrolysis of Urea
Solution of dissolved urease enzyme, urea, & CaCl2 mixed with sand
Urease catalyzes precipitation of CaCO3
CaCO3 grows crystal bridges on soil grains, locking (or cementing) them into place
Cemented soil has sufficient strength & stiffness for many construction purposes
ASU/NASA Space Grant Program
School for Engineering of Matter, Transport, and Energy; School of Sustainable Engineering and the Built Environment
Ira A. Fulton Schools of Engineering

## Slide 7
ASU/NASA Space Grant Program
School for Engineering of Matter, Transport, and Energy; School of Sustainable Engineering and the Built Environment
Ira A. Fulton Schools of Engineering
CaCO3 bridging between soil grains from bio-cementation in a silica 20-30 sand sample
Concave dimple left in CaCO3 bridge after a sand grain presumably broke away in a silica 20-30 sand sample

## Slide 8: Chemical Mechanism
Urease enzyme catalyzes hydrolysis of urea CO(NH2)2 + 3H2O = CO2 + 2NH4+ + 2OH-
Bicarbonate occurs in a high pH environment induced by the enzyme H2O + CO2 = H+ + HCO3-
Bicarbonate forms carbonate under sustained basic conditions H+ + HCO3- + 2OH- = CO32- + 2H2O
Carbonate bonds with calcium & precipitates Ca2+ + CO32- = CaCO3
ASU/NASA Space Grant Program
School for Engineering of Matter, Transport, and Energy; School of Sustainable Engineering and the Built Environment
Ira A. Fulton Schools of Engineering

## Slide 9: Work at ASU
ASU/NASA Space Grant Program
School for Engineering of Matter, Transport, and Energy; School of Sustainable Engineering and the Built Environment
Ira A. Fulton Schools of Engineering
Bio-cement sand column
Test strength after rinsing to remove evaporites
Characterize with SEM, ion chromatography
Quantify weight of CaCO3 precipitate

## Slide 10: Results
Cemented column with 76.8 psi compressive strength
Evidence of increased strength with reduction in reaction speed
ASU/NASA Space Grant Program
School for Engineering of Matter, Transport, and Energy; School of Sustainable Engineering and the Built Environment
Ira A. Fulton Schools of Engineering

## Slide 11: Suggestions for Future Work
Quantify the relationship between % CaCO3 (by weight) & strength
Test the effect of adding CaCO3 seed crystals
Test the effect on finer & coarser grain soils
Evaluate the efficacy of simple urease extraction processes
ASU/NASA Space Grant Program
School for Engineering of Matter, Transport, and Energy; School of Sustainable Engineering and the Built Environment
Ira A. Fulton Schools of Engineering

## Slide 12: Thank you! Comments/Questions?
ASU/NASA Space Grant Program
School for Engineering of Matter, Transport, and Energy; School of Sustainable Engineering and the Built Environment
Ira A. Fulton Schools of Engineering