## Slide 1: Graphene Oxide for Sensing Applications
Christopher Jabczynski
Mentor: Dr. Anthony Muscat – Chemical Engineering
Lauren Peckler – Chemical Engineering
Date: April 16, 2016
Location: Arizona Space Grant Symposium

## Slide 2: Sensing the world around us…
Determine changes in environment
  Accuracy
  Fidelity
Reliability
  Reproducible results
  Reduced maintenance
The Cardio MEMS wireless sensor. Image: IntelFreePress

## Slide 3: Why Graphene oxide (GO)?
X. Zhang, L. Wang, J. Xin, B. I. Yakobson, F. Ding, J. Am. Chem. Soc. 2014, 136, 3040.
Advantages
  One-atom thick carbon nanosheet
  Graphene is very resilient to Volatile Organic Compounds (VOC)
  GO has greater sensitivity to VOC than Graphene
  GO is feasible for large scale manufacturing

## Slide 4: GO Sensor Fabrication
G.O. Dropcast on SI substrate, Muscat lab
Graphene Oxide Suspension, Muscat Group
Suspension of Graphene particles was made in solution to create GO
GO was drop cast onto substrate
Dried casting was then annealed
Annealed G.O. on SI substrate, Muscat lab

## Slide 5: Contacting on the Substrate
Annealed GO was then contacted with silver paste
Corner contacting was used
32 gauge magnetic wire was attached to the silver paste
Four point, and other, contacting was investigated
Four point probe tip from SP4, Muscat lab
Four point contacting on G.O., Muscat lab
Corner contacting on G.O., Muscat lab

## Slide 6: Electrical system setup
Contacted GO was wired to two source meters
The systems was controlled via code written in Labview
Wire was threaded through a stopper in a three neck flask to create a sealed space
Keithly meter - 2700, Tektronik Corp.

## Slide 7: system setup and testing
System was connected to a Schenk line
  Sensor was isolated within the flask
N2 and CO2 where used to cycle and purge the system
Three neck flask, Muscat lab
Schenk line , A.S. Glasware

## Slide 8: Results - Data
Resistance vs. time
Initial measurement with N2
CO2 introduced

## Slide 9: Results - Analysis
Sensor baseline at -80 ohms
  Change from inert gas to organic – magnitude difference of 25 ohms
Further cycling of CO2 and N2 showed trend toward the baseline

## Slide 10: Conclusions
Change in resistance was observed by adding CO2 to the N2 purged chamber
Difference in temperature between gasses
  Possible thermal effects

## Slide 11: Future Work
Create control sensor without GO
  Investigate thermal effects
Use glass to glass seal instead of rubber stopper

## Slide 12: Acknowledgement
NASA Space Grant Consortium
University of Arizona Chemical Engineering Department
Dr. Anthony Muscat
  Muscat group graduate students

## Slide 13: Thank you!