## Slide 1: The Effect of Substrate Choice on Graphene and Oxygen Plasma Interactions
Charlotte K. Johnson, ASU/NASA Space Grant
Christie J. Trimble, Anna M. Zaniewski, and Robert J. Nemanich
Department of Physics, Arizona State University

## Slide 2: Project Introduction
Problem: Exposure to oxygen plasma damages graphene
Could substrate selection mitigate some of the oxygen plasma etching of graphene?

## Slide 3: PMMA transfer method
Before hydrogen furnace treatment
After hydrogen furnace treatment

## Slide 4: Raman Spectrum- Quartz substrate
Chart: Raman Shift (cm-1)

## Slide 5: Raman Spectrum- PPLN substrate
Chart: Raman Shift (cm-1)

## Slide 6: Raman Spectrum- Silicon substrate
Chart: Raman Shift (cm-1)

## Slide 7: Raman Spectrum- Copper substrate
Chart: Raman Shift (cm-1)

## Slide 8: Next Steps
Atomic Layer Deposition Chamber- plasma exposure
Raman Spectroscopy
Analysis
Notes: To remove more of the remaining PMMA, the samples were cleaned in a small tube furnace in an atmosphere of 5% Hydrogen in Argon. This process sublimated much of the remaining PMMA particles off of the surface of the samples.

## Slide 9: Thank you!
Special thanks to the ASU/NASA Space Grant Program, Dr. Anna Zaniewski, Christie Trimble, and the NSL group at ASU

## Slide 10: Questions?

## Slide 11: Graphene monolayer ~1 nm in height atop silicon substrate