## Slide 1: Chemical Passivation of In0.53Ga0.47As(100)
Sanjay Tharmarajah
Yissel Contreras
Anthony Muscat
University of Arizona, Department of Chemical and Environmental Engineering
Arizona Space Grant Symposium
April 22,2017
Tempe, Arizona

## Slide 2: Why III-V Semiconductors
More desirable over Si for high performance transistors due to higher carrier mobilities
In0.53Ga0.47As(100) and InP both have a lattice constant of 5.97 Å
Rapid oxidation in air results in degradation of electrical properties
http://iopscience.iop.org/article/10.1088/0268-1242/28/10/105007
Semiconductor Material | Electron Mobility at ()
Silicon | 1400
GaAs | 8500
In0.53Ga0.47As(100) | 10000
Semiconductor Material | 
Silicon | 1400
GaAs | 8500
In0.53Ga0.47As(100) | 10000
http://www.ioffe.ru/SVA/NSM/Semicond/

## Slide 3: Experimental Approach
Clean semiconductor surface by removing organic material and etching the oxide layer
Deposit a hydrophobic, dense organic layer to prevent oxygen from reacting with the semiconductor surface
oxides
InGaAs(100)
InGaAs(100)
InGaAs(100)
Organic contamination removal using dilute SC1 solution (1:1:10000 v/v NH4OH:H2O2:H2O)
2X (1 min 0.3 M HF etch)
ET deposition
1-Eicosanethiol
(ET)
https://www.revolvy.com/main/index.php?s=Electrochromic%20devices

## Slide 4: A Hydrophobic Surface is Obtained When ET is Deposited
Hydrophobic
Hydrophillic
Chart: Time of Exposure to Atmosphere(min)
| 4 | 8 | 10 | 15 | 20 | 30 | 40 | 50 | 60
20 min in ET | 106.8667 | 106.4333 | 106.1667 | 106.1667 | 103.8667 | 101.7 | 101.7333 | 98.2667 | 95.8333
SC1 clean, HF etch with H20 rinse | 27.7667 | 28.4667 | 26.9667 | 26.9667 | 34.3333 | 31.8333 | 22.5 | 27.1
20 h in ET | 109.63 | 111.33 | 111.87 | 111.7 | 111.37 | 110.67

## Slide 5: Deposition of an Eicosanethiol Monolayer Confirmed by Ellipsometry
Chart: Time of Exposure to Atmosphere (min)
| 4 | 9 | 15 | 20 | 30 | 40 | 50 | 60
Etch and reoxidation control | 7.3667 | 8.6 | 7.7333 | 9.6 | 10.9667 | 9.0667 | 9.5333 | 11.5333
20 min in ET | 20.8333 | 21 | 21.8667 | 22.2667 | 22.5 | 22.9 | 22.6 | 23.1
20 min in ET at 45 C | 21.4333 | 21.6 | 22.0667 | 22.3333 | 22.5667 | 23.0667 | 23.0333 | 23.2333 | 23.4333
20 min in ET at 65 C | 21.4 | 21.67 | 21.93 | 22.3 | 22.47 | 22.57 | 22.83 | 23.2 | 23.4
20 h in ET | 29.9667 | 29.8333 | 30.4 | 31 | 30.1667 | 29 | 30.8 | 30.9333
24 h in ET at 56 C | 29.0667 | 28.5333 | 28.5333 | 28.3333 | 28.6 | 28.5 | 28.7333 | 28.5 | 29.0667
https://en.wikipedia.org/wiki/Ellipsometry
°
°
InP
InGaAs(100)

## Slide 6: An Ordered ET Layer is Formed with 20 min and 20 h Immersions
http://articheck.co.uk/spectroscopy-series-fourier-transformed-infrared/
All samples exposed to air for 4 min before analysis
Higher peak means more dense layer
Interested in wavenumber 2918 and 2850 because of the bond

## Slide 7: Oxide Re-growth is Minimized by ET Deposition
https://wiki.utep.edu/display/~anarayanaswamy/X-Ray+Photoelectron+Spectroscopy
Due the the small escape depth of electrons, x-ray is a surface sensitive technique
A 20 min immersion in ET solution results in a small amount of As oxides are detected
A 20 h immersion in ET solution results in an oxide concentration below XPS detection limits after a 4 min exposure
All samples were exposed to air for 4 min before analysis
c) 20 h ET
b) 20 min ET
a) control

## Slide 8: In Summary
A monolayer of ET was successfully deposited with 20 min and 20 h immersions
The monolayer deposited by the 20 min and 20 h immersion are ordered
20 h immersion in ET solution was more effective in protecting from oxide growth than the 20 min immersion
Future Work:
Analyze various temperatures of ET deposition with XPS and FTIR

## Slide 9: Special Thanks to:

## Slide 10: Thank You!