## Slide 1: Non-Aqueous Surface Passivation of Silicon Germanium
ViAnn Pham1
Stacy Heslop2, Anthony Muscat1
Department of Chemical and Environmental Engineering1
Department of Chemistry and Biochemistry2
University of Arizona
NASA Space Grant Symposium
Arizona State University -Tempe, AZ
Saturday, April 22, 2017

## Slide 2: Motivation
Problem: SiGe and Ge form unstable oxides that inhibit device performance.
  Need to find effective surface passivation method for SiGe and Ge
  Passivation layer = coat of protective material that reduces the amount of chemical reactivity on the surface
2
Material | Hole Mobility (cm2 V/s)
Silicon | 200
Germanium | 450
https://www.androidcentral.com/sites/androidcentral.com/files/styles/xlarge/public/article_images/2015/01/Transistor.png
Del Alamo, Jesús A. "Nanometre-scale electronics with III-V compound semiconductors." Nature 479.7373 (2011): 317-323.

## Slide 3: Background
Use elemental sulfur as passivation reagent.
  Soluble in non-aqueous solvents
  Forms oligomers (chains) on the surface
    Chains could form multilayers which resist reoxidation.
3
Solvent | Solubility (mM)
Water | 1.9 x 10-5
Ethanol | 0.9
Benzene | 88
Solubility of Sulfur in Various Solvents
Jacques Boulegue, Taylor-France Online. Solubility of Elemental Sulufur in Water at 298 K,, 5(1), (2006)

## Slide 4: Objectives
Goal: Develop a non-aqueous process that deposits a sulfur passivation layer on SiGe 75%.
  Passivation layer must protect the surface from reacting with ambient conditions.
SiGe 75%
SiO2/GeO2
SiGe 75%
sulfides
Control
4
Sulfur-passivated surface

## Slide 5: Procedure
Cleaning and etching
SC-1 2 min
  1:1:500 NH4OH:H2O2:H2O
UPW rinse 1 min, N2 dry
HF/HCl Oxide strip 5 min
  1:3:300 HF:HCl:H2O
5
Control
Rinse 30 s in EtOH/benzene, N2 dry
Passivation
(NH4)2S/S in EtOH/S in benzene passivation 20 min
  1:100 (NH4)2S:H2O/S in EtOH/S in benzene
Rinse 30 s in DIW/EtOH/benzene, N2 dry
SiGe 75%
SiO2/GeO2
SiGe 75%
SiGe 75%
Sulfur passivation layer
SiGe 75%
SiGe 75%
SiO2/GeO2
SiGe 75%

## Slide 6: Characterization
Spectroscopic ellipsometry
Measured overlayer (sulfur and oxides) thickness
6
Goniometry
Measured water contact angle
The Leibniz Institute of Polymer Research Dresden
Wikimedia Commons

## Slide 7: Surfaces treated with sulfur in benzene result in 3.6 ± 0.3 nm overlayer thickness.
7
Sulfur in ethanol shows a larger overlayer thickness than (NH4)2S and HF/HCl controls, but layer does not resist oxidation.
Benzene processes deposit a mixture of carbon and sulfur species.

## Slide 8: Surfaces treated with benzene are more hydrophobic than surfaces treated with ethanol.
8
S in benzene: hydrophobic
S in EtOH: hydrophilic
Θ
Passivation Treatments | Water Contact Angle ( ° )
S in benzene | 69.3 ± 0.02
Benzene control | 61.8 ± 0.07
S in EtOH 20 min | 37.1 ± 0.06
EtOH control | 32.3 ± 0.11
(NH4)2S | 19.1 ± 0.06
HCl/HF control | 24.0 ± 0.11
Native oxide | 72.8 ± 0.06
Goniometry Data

## Slide 9: Results
Surfaces treated with sulfur dissolved in alcohols
  Overlayer thickness of 1.4 ± 0.1 nm
  Water contact angle of 37.1 ± 0.1°
9
Surfaces treated with sulfur dissolved in benzene
  Overlayer thickness of 3.6 ± 0.3 nm
  Water contact angle of 69.3 ± 0.02°
SiGe 75%
SiO2/GeO2/sulfides
SiGe 75%
carbon/sulfides

## Slide 10: Conclusions
Surfaces treated with sulfur dissolved in benzene
  Carbon and sulfur species present on surface.
Surfaces with sulfur in benzene  hydrophobic
  Confirms carbon is present on surface
Surfaces with sulfur in alcohols  hydrophilic
  Confirms oxides present on surface
10
Future Work
Analyze sulfur-treated surfaces using x-ray photoelectron spectroscopy (XPS)
  Determine chemical species on surface.
Hybrid approach
  Deposit single layer of sulfur on surface with ammonium sulfide to chemically satisfy dangling surface bonds.
  Deposit multilayers of elemental sulfur in organic solvent on top to form diffusion barrier that resists reoxidation.

## Slide 11: Acknowledgements
Muscat Research Group
NASA/Arizona Space Grant Consortium
Lam Research
11

## Slide 12: Thank you!
12