## Slide 1: Variable Reflectivity Coatings for Optical Propulsion Applications
Joseph. N. Vlastos
Sydney.Taylor & Liping. Wang Ph.D
School of Matter and Transport, Assistant Professor

## Slide 2: Solar Sailing
Advantages
No need to bring fuel
Long lasting
Facts
Uses solar radiation pressure
  Attitude control
  Microscale propulsion

## Slide 3: Utilizing pressure difference
Incident light
Solar Radiation
Pressure Force
Incident light
Reflected light
Solar Radiation
Pressure Force
Torque
Differences in pressure causes torque
Attitude control
Absorption radiation pressure
=
½
Reflectance radiation pressure
Off State = Absorption
Perfectly black service
No reflection
On State = Reflectance
Appears like a mirror
Reflects all wavelengths
No absorption
ON
OFF

## Slide 4: Radiation Pressure Equation
I = Solar extraterrestrial AM 1.5 Spectrum
R = Reflectance
A = Absorption
C = Speed of light
T = Transmittance
A = 1 - R
A + R + T= 1
0
Opaque
Notes: me

## Slide 5: Results
Top mirror metals
Bottom mirror metal
Aluminum
Gold
Tungsten
Gold
Tungsten
Aluminum

## Slide 6: Results
Anti-Reflective coating SiO2
20nm SiO2
100nm SiO2
50nm SiO2
0nm SiO2
Anti-Reflective coating VO2
Au film mirror
Phase change spacer VO2
Tungsten W mirror
Silica wafer
Anti-Reflective coating SiO2
ni= 1
R =
2
n1 – n2
n1 + n2
Reflection

## Slide 7: Fabrication
  6) Anti-Reflective coating SiO2 using Chemical Vapor Depositions
  5) VO2 Using that same method
  Electron Beam Evaporation
  Furnace annealing to oxidize
  4) Au Gold via Electron Beam
3) VO2
  Electron Beam Evaporation
  Furnace annealing to oxidize
2) Tungsten added via Sputtering
1) Starts with a Silica Wafer
Anti-Reflective coating VO2
Au film mirror
Phase change spacer VO2
Tungsten W mirror
Silicon wafer
Anti-Reflective coating 2 SiO2

## Slide 8: Future plans
Characterize the interaction between thermochromic and electrochromic responses
Verify model experimentally
Redesigns for electrical measurements

## Slide 9: Acknowledgments
/ Space Grant
Liping. Wang Ph.D (Mentor)
Sydney Taylor
Desiree Crawl
Hassan Alshehri
My Audience for listening
References
Taylor, Sydney, and Liping Wang. “Vanadium Dioxide-Based Variable Reflectivity Radiation Coatings for Optical Propulsion Applications.” International Astronautical Congress, vol. 67, Sept. 2016.