## Slide 1
Degradation Of Polymeric Materials For Multi-use And Re-use
Meghna Jayaraman
Jen Koevary PhD (Sarver Heart Center, Department of Biomedical Engineering, University of Arizona)
Arizona Space Grant Symposium
April 14th, 2018

## Slide 2: The Problem
Why do we care?
As we look into long term space travel we can’t sustain the current magnitude of waste output
Routinely discarded waste may in fact be a reusable source
Potential Solutions:
  Mandated limits on consumption and consumed materials
    Limited standards of living
    Reduced product efficiency
  Get creative
    Maximize the efficiency of waste management through the recycling and repurposing of materials
    Encourages innovation and competition

## Slide 3: Biomaterials in Tissue Engineering
Biomaterials in tissue engineering have a variety of applications from bone to muscle to skin
  Biodegradable meshes for hernia and cardiac repair
  Biodegradable scaffolds for bone growth and repair
  Biodegradable synthetic skin analogues for burn injuries
It is crucial to characterize the appropriate mechanical parameters of these meshes, to support regeneration without impeding native tissue function
In cardiac applications, for example, a prolonged degradation period and high mechanical strength could restrict ventricular filling

## Slide 4: Objectives
Develop and characterize a variety of methods to repurpose and customize the mechanical properties of pre-manufactured polymer meshes for multi-purpose use on Earth and in space
Our work is designed to elucidate these material characteristics of meshes to aid in handling, engraftment, and biodegradation

## Slide 5: Methods
Two polymeric meshes were explored:
  Polycarbonate and polylactide co-polymer
  Polyglactin 910
Three methods of degradation:
  Hydrolytic degradation (pH 7.4, 37°C)
  Ethylene oxide chemical degradation
  Ultraviolet photolytic degradation (254nm, 15mW)
Tensile testing
  To extract the stiffness and maximum tensile strength
  over the course of degradation

## Slide 6: Hydrolytic Degradation
Simulates in-vitro degradation
  pH 7.4, 37°C
Seven day degradation intervals
Photolytic Degradation
  Ultraviolet light degradation
  254 nm, 15 mW
12 hour exposure periods

## Slide 7: Chemical Degradation
Ethylene oxide sterilization
  12 hour exposures
Three stages:
  Pre-conditioning
    Temperature and humidity controlled to stimulate microorganism growth
  Sterilizer
    EtO gas injection
  De-gasser
    Remove lingering EtO particles

## Slide 8: Tensile Testing
Young’s Modulus (Elastic Modulus)
  Describes the tendency of an object to deform along an axis when opposing forces are applied along that axis
  Stress(F/A) / Strain(mm/mm)
  The more elastic a material, the lower its elastic modulus
Stiffness
  Describes the rigidity of an object, the extent to which it resists deformation to an applied force
  Force(N) / Displacement(mm)
Maximum Tensile Strength
  The maximum force(N) a material can withstand while being stretched before breaking

## Slide 9: Tensile Testing
Kueckelhaus, Maximilian & Philip, Justin & Kamel, Rami & A Canseco, Jose & Hackl, Florian & Kiwanuka, Elizabeth & J Kim, Mi & Wilkie, Ryan & Caterson, Edward & Junker, Johan & Eriksson, Elof. (2014). Sustained Release of Amnion-Derived Cellular Cytokine Solution Facilitates Achilles Tendon Healing in Rats. Eplasty. 14. e29.

## Slide 10: Tensile Testing

## Slide 11: Polycarbonate Co-polymer Stiffness Constant Data

## Slide 12: Polycarbonate Co-polymer Maximum Tensile Strength Data

## Slide 13: Polyglactin910 Co-polymer Stiffness Constant Data

## Slide 14: Polyglactin910 Co-polymer Maximum Tensile Strength Data

## Slide 15: Conclusions
UV degradation is most effective
EtO degradation is least effective
Future Works:
Analyze the effects of combined degradation methods
  Ex: UV and Hydrolytic Degradation of implanted biomaterials in space
Establish a model of polymer degradation to extrapolate potential material properties given a material and environment

## Slide 16: The Big Picture
What does this mean for polymers in space?
EtO degradation and hydrolytic degradation are feasible in space but must be conducted in controlled environments such as metal encasings to limit simultaneous UV degradation
  Aluminum can absorb approximately half the radiation it is exposed to
Light in the range of 200-300 nm is strongly absorbed in the stratosphere by ozone
Transmission of radiation of wavelengths below 290 nm is negligible below 10 km
Effects of photolytic degradation will play an important role in long term space travel
  Negative: difficult to maintain material stability/integrity
  Positive: for re-purposable materials this means that no extra effort needs to be put into degradation

## Slide 17: Acknowledgements
Michele Tang (University of Arizona)
Sherry Daugherty (Sarver Heart Center, University of Arizona)
Jordan Lancaster PhD (Sarver Heart Center, University of Arizona)
Steven Goldman MD (Sarver Heart Center, University of Arizona)

## Slide 18
Thank You