## Slide 1: Investigation of High Shear Granulation Particle Distribution
Michael Lay
Dr. Heather Emady
Arizona Space Grant Symposium, April 14th 2018

## Slide 2: Introduction: Particle Technology
Characterization, handling, and processing of solids unlike fluids
Behavior affected by: friction, density, porosity, structure
Highly empirical field, conducive to research in fundamental phenomena
Example equipment: hoppers, drums, granulators
https://www.911metallurgist.com/blog/lime-slaking-system
https://www.sciencedirect.com/science/article/pii/S0263876215002154

## Slide 3: Introduction: High Shear Granulation
Process of adding liquid binder to powder to create larger granules
Industries: pharmaceuticals, cosmetics, food production, detergent
Studies highlight different regimes, further understanding of processing effects required.
  L/S Ratio
  Impeller Speed
  Drop Height / Impact
  Wet-massing time
This graph I stol from Manogna’s paper, need to include citation for it.

## Slide 4: Experimental: Set-up
Objective: Maximize particles near 1 mm in diameter
Water added to Microcrystalline Cellulose (MCC)
Closely mimic single drop test, slow impellor, low liquid flowrate
Four Liquid/solid ratios, two drop heights
5 minute dry mix, 10 mL/min water addition, 1 hour wetmassing
15 minute samples, sieve analysis

## Slide 5: Results: During Wetmassing
Chart: Time (Minutes)
| 0 | 15 | 30 | 45 | 60
100% L/S Ratio | 0.10959 | 0.10638 | 0.017391 | 0.0098039 | 0
100% L/S Ratio High Drop | 0.076923 | 0.15 | 0.1157 | 0.043478 | 0.030534
110% L/S Ratio | 0.125 | 0.15702 | 0.23636 | 0.26087 | 0.26087
110% L/S Ratio High Drop | 0.078947 | 0.16547 | 0.24409 | 0.24806 | 0.26168
120% L/S Ratio | 0.1125 | 0.2125 | 0.24675 | 0.28049 | 0.28421
120% L/S Ratio High Drop | 0.14615 | 0.26667 | 0.27907 | 0.31496 | 0.24167
130% L/S Ratio | 0.22549 | 0.13514 | 0.12195 | 0.1875 | 0.19481
130% L/S Ratio High Drop | 0.23485 | 0.15044 | 0.12214 | 0.12403 | 0.19672
Weight % of 1 mm particles mm particles formed over time
Ideal L/S ratio near 110-120%
L/S above 130% leads to much larger granules
L/S below 100% lacks sufficient water to make large granules
Increasing drop height has greater effect at lower L/S ratios

## Slide 6: Results: After 60 Minutes
Chart: Minimum Particle Size (mm)
| 1.18 | 1 | 0.85 | 0.71 | 0.6 | 0.5 | 0.35499999999999998 | 0.25 | 0.18 | 0.125 | 0
100% L/S High | 0.2621 | 0.016139 | 0.012912 | 0.0096837 | 0.0077469 | 0.0071014 | 0.069077 | 0.25694 | 0.1827 | 0.1317 | 0.043899
110% L/S High | 0.25279 | 0.095061 | 0.12321 | 0.13224 | 0.11206 | 0.12852 | 0.13542 | 0.012215 | 0.0031864 | 0.0010621 | 0.0042485
120% L/S High | 0.51912 | 0.11852 | 0.1062 | 0.11215 | 0.076466 | 0.03271 | 0.023789 | 0.0055225 | 0.0016992 | 0.0012744 | 0.0025489
130% L/S High | 0.71648 | 0.098901 | 0.070879 | 0.052198 | 0.030769 | 0.013736 | 0.010989 | 0.0032967 | 0.0010989 | 0.00054945 | 0.0010989
100% L/S Low | 0.17767 | 0.0040912 | 0.0040912 | 0.0093513 | 0.019287 | 0.070719 | 0.25833 | 0.24079 | 0.11046 | 0.072 | 0.033
110% L/S Low | 0.27834 | 0.099521 | 0.088345 | 0.14689 | 0.19372 | 0.10644 | 0.067589 | 0.013837 | 0.0021288 | 0.001 | 0.002
120% L/S Low | 0.48732 | 0.13526 | 0.10194 | 0.11735 | 0.079065 | 0.038787 | 0.028344 | 0.0069617 | 0.0019891 | 0.001 | 0.002
130% L/S Low | 0.67047 | 0.11175 | 0.079886 | 0.068474 | 0.035188 | 0.016643 | 0.012363 | 0.0033286 | 0.00095102 | 0.001 | 0
Increased drop height lowered mean particle size for 100% and 110%
Increased drop height had practically no effect on particle distribution for 120% and 130% for particles below 1 mm.
L/S ratio of 120% had largest normalized percentage of particles near 1 mm.
L/S below 100% lacks sufficient water to make large granules
More than 50% of granules formed were larger than 1 mm for L/S ratios of 120% and 130%

## Slide 7: Conclusions: This Investigation
An L/S ratio between 110% to 120% will maximize the normalized percentage of 1 mm granules, but the distribution is broad
Increasing drop height could narrow distribution since greater impact leads to great penetration by the liquid
Drop height has a minimal effect on initial nucleation, and even less effect on final granulation formation

## Slide 8: Conclusions: Future Investigations
Future goal: narrowing size distribution of granules
Investigate size distributions of larger granules e.g. L/S ratio of 130%
Alter impellor speed to verify literature and identify regime type
Further characterize process equipment and solid properties to improve comprehension of underlying phenomena
Ultimate Goal: create model that predicts size and distribution of formed granule

## Slide 9: Acknowledgements
NASA Space Grant
ASU undergraduate research opportunities
Dr. Heather Emady
Manogna Adepu & Tianxiang Gao
Desiree Crawl & Stephanee Germaine

## Slide 10: Thank you
Questions?