## Slide 1: Geopolymers adsorb methicillin-resistant Staphylococcus aureus cells and secreted proteins
Collin Ganser
4-18-2020

## Slide 2: MRSA
Originated from Staphylococcus aureus
Opportunistic pathogen
Antibiotic-resistant “superbug”

## Slide 3
MRSA
Antibiotic resistance crisis
Morbidity and mortality
Economic burden

## Slide 4: Geopolymers (GPs)
Traditionally used in construction and ceramics
Seo lab designed GPs for use as antimicrobial agents
Hypothesized to adsorb materials on pores
Cells and proteins

## Slide 5: Investigation
Question: How effective are geopolymers at adsorbing MRSA secreted proteins?
Hypothesis: mesoGP will adsorb the most MRSA secreted proteins
GPs | Non-coated | Stearic-acid coated
Large pore | MacroGP | SA-macroGP
Small pore | MesoGP | SA-mesoGP

## Slide 6: CFP binding methods
SDS-PAGE
CFP = culture filtrate proteins

## Slide 7: SA-mesoGPs bind the most CFPs
*, P < 0.05; ***, p < 0.001; student’s t test comparing GPs

## Slide 8: Mass spectrometry methods
Analyzed 2 sets of CFP samples
Control CFP
Identified over 100 proteins
Considered proteins present in >50% replicates
Identified bound proteins
Compared control proteins to experimental proteins
CFP incubated with SA-mesoGP

## Slide 9: 58 distinct proteins were bound by SA-mesoGPs
Chart: Distribution of GP-bound proteins by size (kDa)
| Small (< 25) | Medium (25-75) | Large (> 75)
 | 32 | 25 | 1
Chart: Distribution of GP-bound proteins by localization
| Cytoplasm | Ribosome | Unkown | Secreted | Cell surface
 | 17 | 14 | 13 | 10 | 4
Chart: Distribution of GP-bound proteins by function
| Protein production | Virulence | Metabolic processing | Stress response | Cell maintenance | Other biosynthesis
 | 21 | 10 | 10 | 7 | 5 | 5
A
B
C

## Slide 10: Conclusions
Geopolymer effectiveness at adsorbing MRSA secreted proteins
SA-mesoGP >> mesoGP > macroGP > SA-macroGP
  Bound proteins identified by mass spectrometry have diverse size, function, and location

## Slide 11: Future directions
Development of GPs with affinity coatings
Western blot, ELISA, or RT-qPCR with CFP
Hemolysis assays with CFP

## Slide 12: Acknowledgements
Dr. Shelley E. Haydel
John Popovich
The Haydel Lab
Shaojiang Chen
Dr. Dong-Kyun Seo
Dr. Tim Karr
ASU/NASA Space Grant
School of Life Sciences Undergraduate Research (SOLUR) Program

## Slide 13: Thank You!
Questions?