## Slide 1: Characterizing Nanocomposites for Customizable Cartilage Replacements
Presenter: Alexis Hocken
PI: Prof Matthew D. Green
School for Engineering of Matter, Transport and Energy
Arizona State University

## Slide 2: Introduction
Zhan, et al. J. Mech. Behav. Biomed. 2017, 75, 236–243.
1
Nanocomposite applications
  Consumer products
  Construction
  Biomedical applications

## Slide 3: Introduction
This study aims to understand the influence of V-SiO2 and MA-SiO2 loading on the polymerization yield, morphology, and tensile performance
We analyzed samples with 0, 3.8, 7.4, 10.7, and 13.8 wt% silica nanoparticles
Hocken, et al. Industrial & Engineering Chemistry Research. 2019, 58 (32).
2
SiO2
SiO2
MA-SiO2
V-SiO2
SiO2
Photocuring Mechanism
Unfunctionalized SiO2
Phase 1:
Phase 2:

## Slide 4: Background
Hocken, et al. Industrial & Engineering Chemistry Research. 2019, 58 (32).
Cross-Linking Reaction of PEGDA Initiated by DMPA under UV Light
3
Cross-Linking Reaction of PEGDA with V-SiO2
Cross-Linking Reaction of PEGDA with MA-SiO2

## Slide 5: Confirming Gel Fraction
*Hocken, et al. Industrial & Engineering Chemistry Research. 2019, 58 (32).
Chart: Nanoparticle Concentration (wt%)
| 0 | 3.8 | 7.4 | 10.7 | 13.8
SiO2 | 98 | 95 | 93 | 91 | 91
MA-SiO2 | 98 | 97.28 | 97.4267 | 96.48 | 98.24
V-SiO2 | 98 | 94.8767 | 96.45 | 98.7567 | 96.3933
SiO2*
MA-SiO2
V-SiO2
SiO2
SiO2
MA-SiO2
V-SiO2
4
Notes: by scavenging radicals, limiting diffusion, or simply by diluting the concentration of monomer in the system

## Slide 6: Determining Mechanical Properties
*Hocken, et al. Industrial & Engineering Chemistry Research. 2019, 58 (32).
SiO2*
MA-SiO2
V-SiO2
SiO2*
MA-SiO2
V-SiO2
SiO2
SiO2
MA-SiO2
V-SiO2
5
Notes: by scavenging radicals, limiting diffusion, or simply by diluting the concentration of monomer in the system

## Slide 7: Conclusions & Future Work
SiO2
SiO2
SiO2
For this V-SiO2 and MA-SiO2 :
  Investigate composite composition through TGA and DMA
  Formalize a manuscript and submit for publication
Moving further, we could investigate the effects of :
  Other nanoscale additives
    Other surface compositions
    Other sizes
  Cross-linker molecular weight
  Photocatalysts
6

## Slide 8: Acknowledgements
PI: Dr. Matthew D. Green
ASU/NASA Space Grant Program
Fellow Labmates: Dr. Yi Yang, Dr. Meng Wang, Jason Lee, Mani Korah, Brad Grim, Hoda Shokrollahzadeh
Dr. Frederick L. Beyer and Dr. Brian F. Morgan at the Army Research Lab
7