## Slide 1
Characterization of Defects in Crystalline Optical Coatings
Breck Meagher₁, Mentor: Dr. E. Gretarsson₂, Dr. A. Markosyan₃, Dr. A. Gretarsson₄
Department of Physics and Astronomy₁,₄, Department of Aerospace Engineering₂, Stanford LIGO Group₃
2023 Arizona NASA Space Grant Statewide Symposium
Partner

## Slide 2
LIGO
Amorphous, dielectric coatings
  Highly reflective
  Minimal optical loss
[1]
Figure 2. Two LIGO ‘Test Masses’, LIGO Optics Caltech
Figure 1. Basic Interferometer Diagram, LIGO Caltech
[2]
2

## Slide 3
AlGaAs Coatings
Figure 3. Adapted from “Typical Semiconductor Supermirror”, Garret Cole, et. al.
[3]
Monocrystalline Aluminum Gallium Arsenide
10x reduction in thermal noise
Defects despite high purity
3

## Slide 4
Sample Damage
Coating Damage
Imaging the Defects
4

## Slide 5
Types of Defects
Damage (<1 μm)
Debris on surface
6
Pyramids (~1 μm)
Raised above surface
Shells (~5 μm)
Indents into surface

## Slide 6
Absorption
SEM data plotted with overlapping absorption data
14,710 cts
10,320 cts
23,810 cts
8

## Slide 7
Conclusions
  Absorption data can be correlated to SEM measurements
  Surface defects are characterizable
Future Plans
  Obtain size and distribution characteristics over a large area
  Analyze additional samples
Conclusions & Future Plans
9