## Slide 1: Laboratory Measurements of the Thickness, Index of Refraction, and Density of Ices Important to Planetary Science
Moises Gomez
Advisor: Dr. Stephen Tegler
Department of Astronomy and Planetary Science

## Slide 2
Methane ice on Pluto mapped by the New Horizon’s spacecraft. (Source: NASA)

## Slide 3
Deposited ice mixtures of CH4 and N2 onto a substrate inside of vacuum chamber.
Pressure around 5 * 10-9 torr and temperatures ranging from 10-30K.
Thin films of ice < 1 micron thick.
*Picture of the entire chamber*

## Slide 4: Lab Setup (Pt. 1 QCM, Las
Laser fringe data obtained from a N2 and CH4 (ratio 60:40) ice mixture at 10K.

## Slide 5
QCM frequency data obtained from a N2 and CH4 (60:40) at 10K.
Quartz Crystal Microbalance (QCM)

## Slide 6: Optical Constants of CH4 and N2 ice at 10K
Sample | Ratio | Thickness (microns) | Density (g/cm3) | Compared Density (g/cm3) | nvis | Compared nvis
N2:CH4 | 0:100 | 0.44 | 0.49 | 0.49* | 1.32 | 1.30*
N2:CH4 | 60:40 | 0.61 | 0.71 | — | 1.33 | —
N2:CH4 | 80:20 | 0.95 | 0.93 | — | 1.28 | —
N2:CH4 | 100:0 | 1.26 | 0.98 | 0.95* | 1.22 | 1.22*
*Satorre, M. Á., et al. "Density of CH4, N2 and CO2 ices at different temperatures of deposition." Planetary and Space Science 56.13 (2008): 1748-1752.

## Slide 7: Thank You!
Acknowledgement to:
NASA/NAU Space Grant
Dr. Stephen Tegler
Dr. Will Grundy
Aidan Madden-Watson