## Slide 1: Hydrogen Production and Storage in CaTiO3 Perovskite at Mantle-Related High Pressures
Ava Campbell
18 April 2026
AZ NASA Space Grant
Statewide Student Research Symposium
Advisor: Dr. Sang-Heon Dan Shim

## Slide 2: Introduction
CaTiO3 perovskite is known to split water into H2 and O2 using UV light as a catalyst at 1 bar (Passi and Pal, 2021)
Preliminary experiments indicate that heat can replace UV light at high pressures
CaTiO3 → CaTiO2.5 + 0.25 O2
CaTiO2.5 + 0.5 H2O → CaTiO3 + 0.5 H2
∆

## Slide 3: Introduction
CaTiO3 perovskite is known to split water into H2 and O2 using UV light as a catalyst at 1 bar (Passi and Pal, 2021)
Preliminary experiments indicate that heat can replace UV light at high pressures
CaTiO3 → CaTiO2.5 + 0.25 O2
CaTiO2.5 + 0.5 H2O → CaTiO3 + 0.5 H2
∆
PT

## Slide 4: Introduction
For CaTiO3 perovskite to split water:
Ti’s ability to change oxidation states
Crystal Structure
For Fe-bearing MgSiO3 and CaSiO3 perovskites:
Fe’s ability to change oxidation states
Crystal Structure

## Slide 5: Methods – High-Pressure Experiments
“Big Blue” ASU’s 1100-ton multi-anvil press
Assembly inside 8 tungsten-carbide cubes and connected to thermocouple (red and white wires) to measure temperature.
Assembly used for experiments. Sample is loaded into a welded
Pt capsule.
1 in

## Slide 6: Methods – Spectroscopic Analysis
Recovered sample capsule. Capsule is cut in half (red dotted line) and Raman is measured in the middle of the sample.
A piece of sample is removed from the recovered sample capsule and double polished to 100 micron thickness to prepare it for IR measurements.
capsule
sample
MgO from assembly
Raman and IR are vibrational spectroscopy techniques. These measure the H-H bond (along with others such as O-H)
H2 stretching vibration

## Slide 7: Results and Discussion – Raman H2 Band Shifting
H2 peak separation of
15 GPa sample: 42 cm-1
10 GPa sample: 50 cm-1
750 C sample: 65 cm-1

## Slide 8: Results and Discussion – IR H2 Band Shifting
O-H stretching-bending combination modes tend to occur ≥4200 cm-1 (Ohlhorst et al., 2001; Bishop et al., 2002; Efimov, 2003; Wu et al., 2021)

## Slide 9: Discussion – H2 Storage vs H2O Splitting
Across all samples, the 10GPa/500C sample has the most intense H2 band in both Raman and IR
The 10GPa/500C PT condition maximizes both water splitting and H2 storage efficiency
P/T
water splitting or H2 storage efficiency
water splitting or H2 storage efficiency
10GPa, 500C
P/T

## Slide 10: Conclusion
This work varied the synthesis PT conditions for the CaTiO3 water splitting reaction and subsequent H2 storage within the CaTiO3 crystal structure.
Based on the H2 peak shifting in both Raman and IR, we interpret that the preferred crystallographic site of H2 in CaTiO3 perovskite changes based on the pressure and temperature conditions.

## Slide 11: Conclusion
This work varied the synthesis PT conditions for the CaTiO3 water splitting reaction and subsequent H2 storage within the CaTiO3 crystal structure.
Based on the H2 peak shifting in both Raman and IR, we interpret that the preferred crystallographic site of H2 in CaTiO3 perovskite changes based on the pressure and temperature conditions.

## Slide 12: Future Work
In situ IR measurements while heating
Determine if observed peaks at higher wavenumbers are associated with H2 or some OH-related band
Computational work to calculate crystallographic site and corresponding Raman/IR signal
Calculated spectra can provide a better understanding of how the preferred crystallographic site of H2 changes with pressure and temperature

## Slide 13: Geologic Implications
Hand (2023)
CaTiO3
H2O
H2
+ H2

## Slide 14: Acknowledgements
I would like to thank Dr. Shim for advising and guiding me in this project; Dr. Shock for providing his expertise and support in this project; Drs. Chen and Kim for training me on high-pressure techniques, including multi-anvil press and Raman; Dr. Shim’s lab group for listening and providing feedback and support for not only this presentation, but this project over the last 2 years; FORCE facility for use of their multi-anvil press and support in training me; Eyring Materials Center for training on and use of their IR; and NASA Space Grant for providing financial support and opportunities to present this work in a variety of settings

## Slide 15: References
Bishop, J.; Murad, E.; Dyar M. D. The Influence of Octahedral and Tetrahedral Cation Substitution on the Structure of Smectites and Serpentines as Observed through Infrared Spectroscopy. Clay Miner. 2002, 37 (4), 617–628. https://doi.org/10.1180/0009855023740064.
Efimov, A. M.; Pogareva, V. G.; Shashkin, A. V. Water-Related Bands in the IR Absorption Spectra of Silicate Glasses. J. Non-Cryst. Solids 2003, 332 (1), 93–114. https://doi.org/10.1016/j.jnoncrysol.2003.09.020.
Hand, E. Hidden Hydrogen: Earth may hold vast stores of renewable carbon-free fuel. Science. 2023, 379(6633). https://doi.org/10.1126/science.adh1460
Moine, B. N.; Bolfan-Casanova, N.; Radu, I. B.; Ionov, D. A.; Costin, G.; Korsakov, A. V.; Golovin, A. V.; Oleinikov, O. B.; Deloule, E.; Cottin, J. Y. Molecular Hydrogen in Minerals as a Clue to Interpret ∂D Variations in the Mantle. Nat. Commun. 2020, 11 (1), 3604. https://doi.org/10.1038/s41467-020-17442-8.
Ohlhorst, S.; Behrens, H.; Holtz, F. Compositional Dependence of Molar Absorptivities of Near-Infrared OH- and H2O Bands in Rhyolitic to Basaltic Glasses. Chem. Geol. 2001, 174 (1), 5–20. https://doi.org/10.1016/S0009-2541(00)00303-X.
Passi, M.; Pal, B. A Review on CaTiO3 Photocatalyst: Activity Enhancement Methods and Photocatalytic Applications. Powder Technol. 2021, 388, 274–304. https://doi.org/10.1016/j.powtec.2021.04.056.
Wu, S.; He, M.; Yang, M.; Zhang, B.; Wang, F.; Li, Q. Near-Infrared Spectroscopy Study of Serpentine Minerals and Assignment of the OH Group. Crystals 2021, 11 (9), 1130. https://doi.org/10.3390/cryst11091130.