## Slide 1: Measuring Mechanical Properties of Thin Optical Coatings
Elaine Rhoades
Mentors: Dr. Zanolin, Embry-Riddle Aeronautical University
Dr. Gretarsson, Embry-Riddle Aeronautical University
April 12, 2014 NASA Space Grant Symposium

## Slide 2: Experimental Setup
Use a transducer to emit and sense reflections of a 0.4 GHz, 10 ns acoustic pulse from the surface of a sample.
Materials affect the reflected amplitude differently
Reflected amplitude contains information about the Young’s Modulus
Image credit: Dr. Andri Gretarsson, ERAU

## Slide 3: Experimental Setup
Water absorption likely has a temperature dependence
Experimental setup has a thermocouple inserted between the piezo and spacers, which allows us to monitor the water’s temperature during data collection
Photo credit: Dr. Andri Gretarsson, ERAU

## Slide 4: Data
Remove noise in the signal by band limiting (cut |FFT|)
Exponential form results from water
absorption and
other losses
Image credit: Justin Weber, ERAU

## Slide 5: Updates to the acoustics analysis
Automated the data windowing process
Introduced the use of a Tukey window to remove high frequency components
Introduced error propagation

## Slide 6: Y Estimate Depends on σ

## Slide 7: Nanoindentation

## Slide 8: Comparison of Acoustics and Nanoindentation
Colored background is the acoustics chi-squared plot
Bold dashed line is the nanoindentation fit
Solid white lines are the errors in the nanoindentation fit

## Slide 10: Samples
Silica
Sapphire
Silicon cantilevers (borrowed from Glasgow group)
Silicon windows
Single-layer tantala coatings, base silica
Photo credit: Dr. Andri Gretarsson, ERAU